## Slide 1: Diffraction
When “scattering”
is not random

## Slide 2
detector
sample
detector
x-ray beam
scattering

## Slide 4: Scattering: atom by atom
h index
intensity

## Slide 5: Scattering: atom by atom
h index
intensity

## Slide 6: Scattering: atom by atom
h index
intensity

## Slide 7: Scattering: atom by atom
h index
intensity

## Slide 8: Scattering: atom by atom
h index
intensity

## Slide 9: Scattering: atom by atom
h index
intensity

## Slide 10: Scattering: atom by atom
h index
intensity

## Slide 11: Scattering: atom by atom
h index
intensity

## Slide 12: Scattering: atom by atom
h index
intensity

## Slide 13
sample
detector
x-ray beam
scattering

## Slide 14
sample
detector
x-ray beam
scattering

## Slide 15
sample
detector
x-ray beam
scattering

## Slide 16
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 17
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 18
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 20
scattering from a structure
sample
detector

## Slide 21
forward Fourier Transform
inverse Fourier Transform
no phase

## Slide 22
scattering from a structure
colored by phase
sample
detector
inverse Fourier Transform

## Slide 23
scattering from a lattice
colored by phase
sample
detector

## Slide 24
scattering from a lattice
colored by phase
sample
detector

## Slide 25
scattering from a lattice
colored by phase
sample
detector

## Slide 26
scattering from a crystal structure
colored by phase
sample
detector

## Slide 27: lysozyme: real and reciprocal

## Slide 28: X-ray data are 3D!

## Slide 29: Ewald's construction
Ewald sphere
(h,k,l)

## Slide 30: Ewald's construction
Ewald sphere
(h,k,l)
d*

## Slide 31: Ewald's construction
Ewald sphere
spindle axis
(h,k,l)
d*

## Slide 32: Ewald's construction
Ewald sphere
spindle axis
Φ circle
(h,k,l)

## Slide 33: Ewald's construction
Ewald sphere
spindle axis
Φ circle
(h,k,l)

## Slide 34: Ewald's construction
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)

## Slide 35: Ewald's construction
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*

## Slide 36: Ewald's construction
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*
θ
λ = 2 d sin(θ)

## Slide 37: Ewald's construction
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*

## Slide 38: mosaic spread
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
λ*
λ*
d*
d*

## Slide 39: mosaic spread
Ewald sphere
spindle axis
Φ circle
diffracted rays
(h,k,l)
d*
d*

## Slide 40: mosaic spread = 0 º

## Slide 41: mosaic spread = 0.1º

## Slide 42: mosaic spread = 0.2º

## Slide 43: mosaic spread = 0.4º

## Slide 44: mosaic spread = 0.6º

## Slide 45: mosaic spread = 0.8º

## Slide 46: mosaic spread = 1.0º

## Slide 47: mosaic spread = 1.5º

## Slide 48: mosaic spread = 2.0º

## Slide 49: mosaic spread = 2.5º

## Slide 50: mosaic spread = 3.2º

## Slide 51: mosaic spread = 6.4º

## Slide 52: mosaic spread = 12.8º

## Slide 53
Ewald’s “mosaic” picture

## Slide 54
Ewald’s “mosaic” picture

## Slide 55
Ewald’s “mosaic” picture
What is
this stuff?

## Slide 56
source
detector
d
atom #1
atom #2
“near”-ly Bragg’s Law

## Slide 57: mosaic block = “coherence length”
James R. W. (1962) Optical Principles of the Diffraction of X rays. Ox Bow press.

## Slide 58
“crystal”
detector
x-ray beam
peak
intensity
integrated
intensity
Scattering: line of atoms

## Slide 59: Scattering: line of atoms
10 atoms
0.1 μm
50 atoms
0.5 μm
100 atoms
1 μm
200 atoms
2 μm
300 atoms
3 μm
400 atoms
4 μm
500 atoms
5 μm
1000 atoms
10 μm
position on detector (mm)
intensity (photons/SR/atom)

## Slide 60: Scattering: line of atoms
B factor
mosaic
spread
peak intensity (photons/SR)
number of atoms in line
mosaic
block
size
depends on detector distance !!!
integrated intensity never changes

## Slide 61
Ewald’s “mosaic” picture
What is
this stuff?

## Slide 62
Darwin’s original picture

## Slide 63
“mosaicity” with visible light

## Slide 64: mosaic spread = 12.8º

## Slide 65: Now What?
10 Å

## Slide 66: Resolution
http://bl831.als.lbl.gov/~jamesh/movies/resolution.mpeg

## Slide 67: What is “disorder”?

## Slide 68: What is “disorder”?

## Slide 69: What is “disorder”?

## Slide 70: What is “disorder”?
order
order
disorder
B-factor

## Slide 71: “B” factors
ATOM 122 N LEU A 13 -3.244 25.808 19.998 1.00 16.96 N
ATOM 123 CA LEU A 13 -2.877 25.448 21.355 1.00 15.29 C
ATOM 124 C LEU A 13 -2.792 23.966 21.561 1.00 17.54 C
ATOM 125 O LEU A 13 -1.814 23.493 22.143 1.00 16.35 O
ATOM 126 CB LEU A 13 -3.907 26.164 22.268 1.00 18.72 C
ATOM 127 CG LEU A 13 -3.577 25.982 23.738 1.00 21.19 C
ATOM 128 CD1 LEU A 13 -2.283 26.820 24.019 1.00 19.43 C
ATOM 129 CD2 LEU A 13 -4.702 26.474 24.639 1.00 24.65 C
ATOM 130 N SER A 14 -3.677 23.149 20.979 1.00 15.96 N
ATOM 131 CA SER A 14 -3.646 21.711 21.061 1.00 18.26 C
ATOM 132 C SER A 14 -2.373 21.203 20.360 1.00 18.71 C
ATOM 133 O SER A 14 -1.747 20.315 20.930 1.00 17.47 O
ATOM 134 CB SER A 14 -4.875 21.077 20.419 1.00 17.62 C
ATOM 135 OG ASER A 14 -4.825 19.665 20.388 0.50 20.89 O
ATOM 136 OG BSER A 14 -6.027 21.408 21.164 0.50 18.67 O
ATOM 137 N LYS A 15 -2.045 21.772 19.215 1.00 18.03 N
ATOM 138 CA LYS A 15 -0.799 21.361 18.555 1.00 18.12 C
ATOM 139 C LYS A 15 0.446 21.707 19.351 1.00 18.81 C
ATOM 140 O LYS A 15 1.400 20.948 19.411 1.00 17.77 O
ATOM 141 CB LYS A 15 -0.700 22.034 17.177 1.00 14.49 C
ATOM 142 CG LYS A 15 -1.727 21.368 16.256 1.00 16.12 C
ATOM 143 CD LYS A 15 -1.663 22.147 14.936 1.00 19.40 C
ATOM 144 CE ALYS A 15 -2.725 21.614 13.986 0.50 17.42 C
ATOM 145 CE BLYS A 15 -1.750 21.211 13.750 0.50 17.01 C
ATOM 146 NZ ALYS A 15 -2.346 21.674 12.559 0.50 18.61 N
ATOM 147 NZ BLYS A 15 -3.052 20.513 13.741 0.50 18.76 N

## Slide 72: “B” factors
B = 8π2 ux2
ux = RMS variation perpendicular to plane

## Slide 73
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 74
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 75
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 76
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 77: “B” factors
B ≈ 4d2 + 12
essentially, the “resolution” of an atom
d = resolution in Å

## Slide 78
What causes disorder?
Thermal vibration (B factor)
Micron-scale cracks (mosaic spread)
Stress and strain (sample handling)
Radiation Damage

## Slide 79
Radiation damage
Howells, et al. (2009) J. Electron Spectrosc. Relat. Phenom. 170, 4-12.

## Slide 80: Completeness: missing wedge
http://bl831.als.lbl.gov/~jamesh/movies/osc.mpeg

## Slide 81
maximum tolerable dose (MGy)
1 2 3 5 7 10 20 40 70 100
1
10
100
103
resolution (Å)
Howells et al. (2009) J. Electron. Spectrosc. Relat. Phenom. 170 4-12
Global damage

## Slide 82
resolution (Å)
maximum tolerable dose (MGy)
1 2 3 5 7 10 20 40 70 100
1
10
100
103
Howells et al. (2009) J. Electron. Spectrosc. Relat. Phenom. 170 4-12
Global damage
10 MGy/Å

## Slide 83: 10 MGy/Å
what the is a MGy?
http://bl831.als.lbl.gov/
damage_rates.pdf
Holton J. M. (2009) J. Synchrotron Rad. 16 133-42

## Slide 84
How long will my crystal last?

## Slide 85
Damage is done
by dose (MGy)
proportional to photons/area
not time
not heat

## Slide 86: Minimum size for complete data set
molecular weight
crystal diameter (μm)
100 Da 1 kDa 10 kDa 100 kDa 1 MDa 10 MDa
1 Å
X-rays
2 Å
spots
B = 24
50%
solvent
Holton & Frankel (2010) Acta D 66 393-408.

## Slide 87
Holton & Frankel (2010) Acta D 66 393-408.

## Slide 88: Ratio of scattering to absorption
Atomic number (Z)
Elastic/photoelectric cross section

## Slide 89: How do the X-rays interact with my crystal?

## Slide 90: Where do photons go?
beamstop
Transmitted (98%)
Protein
1A x-rays

## Slide 91: Photonuclear absorption

## Slide 92: Photonuclear absorption

## Slide 93: Elastic scattering

## Slide 94: Elastic scattering

## Slide 95: How big is an atom?
C
1 Ångstrom (Å)
1 nanometer (10-9 m)
N
O
S
H
U

## Slide 96: How big is an atom?
U
C
N
O
S
H
as seen by X-rays

## Slide 97: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
Protein
1A x-rays

## Slide 98: Elastic scattering

## Slide 99: Inelastic scattering

## Slide 100: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
Protein
1A x-rays

## Slide 101: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Protein
1A x-rays

## Slide 102: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Protein
1A x-rays
Re-emitted (99%)
Absorbed (~0%)

## Slide 103: Photoelectric absorption

## Slide 104: Photoelectric absorption
e-
+

## Slide 105: Fluorescence
+

## Slide 106: Fluorescence
e-
+

## Slide 107: Fluorescence-based x-ray sources

## Slide 108: What limits the source?
Fluorescence-based source:
Thermal distortion of anode
Accelerator-based source
Quality of optics
Electric bill

## Slide 109: Auger emission
+

## Slide 110: Auger emission
++
e-

## Slide 111: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Protein
1A x-rays
Re-emitted (99%)
Absorbed (~0%)

## Slide 112: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Photoelectric (87%)
Protein
1A x-rays
Re-emitted (99%)
Absorbed (~0%)

## Slide 113: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Photoelectric (87%)
Protein
1A x-rays
Re-emitted (~0%)
Absorbed (99%)
Re-emitted (99%)
Absorbed (~0%)

## Slide 114: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
useful/absorbed energy: 7.3%
inelastic scattering (7%)
Photoelectric (87%)
Protein
1A x-rays
Re-emitted (~0%)
Absorbed (99%)
Re-emitted (99%)
Absorbed (~0%)

## Slide 115: Photoelectric absorption

## Slide 116: Photoelectric absorption
e-
+

## Slide 117: Secondary ionization
e-

## Slide 118: Secondary ionization
e-
e-
+

## Slide 119: Sample atoms

## Slide 120: Sample atoms

## Slide 121: Primary ionization
e-
+

## Slide 122: Secondary ionizations
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+

## Slide 123: Ionization track
e-
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
+
e-
+

## Slide 124: Ionization track
e-
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
+
e-
+

## Slide 125: Ionization track

## Slide 126: Ionization track

## Slide 127: Ionization track
~ 3 microns!

## Slide 128: Excitation
e-

## Slide 129: Excitation
e-

## Slide 130: Excitation
e-

## Slide 131: Excitation

## Slide 132: Electron attachment
e-

## Slide 133: Electron attachment
-

## Slide 134: Solvated electron
e-

## Slide 135: Solvated electron
e-

## Slide 138: Excitation transfer

## Slide 139: Excitation transfer
UV photon

## Slide 140: Excitation transfer

## Slide 141: Excitation transfer
Förster transfer
r-6

## Slide 142: Excitation transfer

## Slide 143: t = 0 s

## Slide 144: t ≈ 10-15 s
-
e-
+
+

## Slide 145: Timescales of radiation damage
Garret et. al. (2005) Chem. Rev. 105, 355-389
LCLS
AS
bunch

## Slide 146: What does all that absorbed energy do?

## Slide 147
D1/2 >> 1012 Gy
D1/2 ~ 10 Gy

## Slide 148: Sodium Chloride is Immortal!
D1/2 > 1 GGy

## Slide 149: Sodium acetate trihydrate
D1/2 = 15 MGy
resolution: 0.92 Å
avg B: ~ 0
R/Rfree: ~4%
C2/c

## Slide 150: lowest-angle spot: (1,1,0) 7.7 Å
integrated spot intensity
dose (MGy)

## Slide 174
Holton (2009) J. Synchrotron Rad. 16 133-42
Specific damage rates
world records:
MGy reaction reference
~45 global damage Owen et al. (2006)
5 Se-Met Holton (2007)
4 Hg-S Ramagopal et al. (2004)
3 S-S Murray et al. (2002)
1 Br-RNA Olieric et al. (2007)
? Cl-C ???
0.5 Mn in PS II Yano et al. (2005)
0.02 Fe in myoglobin Denisov et al. (2007)

## Slide 175: % error from rad dam
Riso (%)
change in dose (MGy)
data taken from Banumathi, et al. (2004) Acta Cryst. D 60, 1085-1093.

## Slide 176: % error from rad dam
Riso (%)
change in dose (MGy)
data taken from Banumathi, et al. (2004) Acta Cryst. D 60, 1085-1093.
Riso ≈ 0.7 %/MGy

## Slide 177: The “non-isomorphism” problem
Rel. Humidity: 84.2% vs 71.9%
Riso = 44.5%
RMSD = 0.18 Å

## Slide 178: opened drop: you have ~30 seconds!
equilibrated drop

## Slide 179: opened drop: you have ~30 seconds!
oil

## Slide 180: oiled drop: you have ~3 hours
oil

## Slide 181: oil is your friend

## Slide 182: signal vs noise
“photon counting”
Read-out noise
Shutter jitter
Beam flicker
spot shape
radiation damage
σ(N) = sqrt(N)
rms 11.5 e-/pixel
rms 0.57 ms
0.15 %/√Hz
pixels? mosaicity?
B/Gray?

## Slide 183: signal vs noise
fractional noise
“photon counting”
constant noise
σ(I) = k x I “% error”
σ(I) = k x sqrt(I)
σ(I) = k

## Slide 184: signal vs noise
fractional noise
“photon counting”
constant noise
σ(I) = k x I “% error”
σ(I) = k x sqrt(I)
σ(I) = k

## Slide 185: signal vs noise
fractional noise
“photon counting”
constant noise
σ(I) = k x I “% error”
σ(I) = k x sqrt(I)
σ(I) = k

## Slide 186: Optimal exposure time (faint spots)
thr Optimal exposure time for data set (s)
tref exposure time of reference image (s)
bgref background level near weak spots on
reference image (ADU)
bg0 ADC offset of detector (ADU)
bghr optimal background level (via thr)
σ0 rms read-out noise (ADU)
gain ADU/photon
m multiplicity of data set (including partials)
adjust exposure
so this is ~100

## Slide 187: Adding noise

## Slide 188: Adding noise
12 + 12 = 1.42

## Slide 189: Adding noise
12 + 12 = 1.42
32 + 12 = 3.22
σtotal2 = σ12 + σ22

## Slide 190: Adding noise
12 + 12 = 1.42
32 + 12 = 3.22
σtotal2 = σ12 + σ22

## Slide 191: Adding noise
12 + 12 = 1.42
32 + 12 = 3.22
σtotal2 = σ12 + σ22

## Slide 192: Adding noise
12 + 12 = 1.42
32 + 12 = 3.22
102 + 12 = 10.052

## Slide 193: signal vs noise
fractional noise
“photon counting”
constant noise
σ(I) = k x I “% error”
σ(I) = k x sqrt(I)
σ(I) = k

## Slide 194
sample
x-ray beam
anomalous scattering
detector

## Slide 195
sample
detector
x-ray beam
anomalous scattering

## Slide 196
sample
x-ray beam
anomalous scattering
detector

## Slide 197
sample
detector
x-ray beam
anomalous scattering

## Slide 198
sample
detector
x-ray beam
anomalous scattering

## Slide 199
anomalous signal
Crick, F. H. C. & Magdoff, B. S. (1956) Acta Crystallogr. 9, 901-908.
Hendrickson, W. A. & Teeter, M. M. (1981) Nature 290, 107-113.
# sites
MW (Da)
ΔF
F
≈ 1.2 f”
√
f” | Element
0.5 | S P
4 | Se Br Fe
10 | Hg Gd Au Pt
World record!
ΔF/F = 0.5%
Wang, Dauter & Dauter (2006) Acta Cryst. D 62, 1475-1483.

## Slide 200: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 201: Darwin’s Formula
I(hkl) - photons/spot (fully-recorded)
Ibeam - incident (photons/s/m2 )
re - classical electron radius (2.818x10-15 m)
Vxtal - volume of crystal (in m3)
Vcell - volume of unit cell (in m3)
λ - x-ray wavelength (in meters!)
ω - rotation speed (radians/s)
L - Lorentz factor (speed/speed)
P - polarization factor
(1+cos2(2θ) -Pfac∙cos(2Φ)sin2(2θ))/2
A - attenuation factor
exp(-μxtal∙lpath)
F(hkl) - structure amplitude (electrons)
C. G. Darwin (1914)
P A | F(hkl) |2
I(hkl) = Ibeam re2
Vxtal
Vcell
λ3 L
ωVcell

## Slide 202: Darwin’s Formula
I(hkl) - photons/spot (fully-recorded)
Ibeam - incident (photons/s/m2 )
re - classical electron radius (2.818x10-15 m)
Vxtal - volume of crystal (in m3)
Vcell - volume of unit cell (in m3)
λ - x-ray wavelength (in meters!)
ω - rotation speed (radians/s)
L - Lorentz factor (speed/speed)
P - polarization factor
(1+cos2(2θ) -Pfac∙cos(2Φ)sin2(2θ))/2
A - attenuation factor
exp(-μxtal∙lpath)
F(hkl) - structure amplitude (electrons)
C. G. Darwin (1914)
P A | F(hkl) |2
I(hkl) = Ibeam re2
Vxtal
Vcell
λ3 L
ωVcell

## Slide 203: attenuation factor
Bouguer, P. (1729). Essai d'optique sur la gradation de la lumière.
Lambert, J. H. (1760). Photometria: sive De mensura et gradibus luminis, colorum et umbrae. E. Klett.
Beer, A. (1852)."Bestimmung der Absorption des rothen Lichts in farbigen Flüssigkeiten", Ann. Phys. Chem 86, 78-90.
A = = exp(-μt)
IT
Ibeam
t
μ

## Slide 204: attenuation factor
Bouguer, P. (1729). Essai d'optique sur la gradation de la lumière.
Lambert, J. H. (1760). Photometria: sive De mensura et gradibus luminis, colorum et umbrae. E. Klett.
Beer, A. (1852)."Bestimmung der Absorption des rothen Lichts in farbigen Flüssigkeiten", Ann. Phys. Chem 86, 78-90.
A = = exp(-μ(tin+ tout))
IT
Ibeam
t
tin
tout
A = = exp(-μt)
IT
Ibeam
μ

## Slide 205: attenuation factor
Bouguer, P. (1729). Essai d'optique sur la gradation de la lumière.
Lambert, J. H. (1760). Photometria: sive De mensura et gradibus luminis, colorum et umbrae. E. Klett.
Beer, A. (1852)."Bestimmung der Absorption des rothen Lichts in farbigen Flüssigkeiten", Ann. Phys. Chem 86, 78-90.
A = = exp(-μ(tin+ tout))
IT
Ibeam
tin
tout
tin
tout
tin
tout
μ

## Slide 206: attenuation factor
Bouguer, P. (1729). Essai d'optique sur la gradation de la lumière.
Lambert, J. H. (1760). Photometria: sive De mensura et gradibus luminis, colorum et umbrae. E. Klett.
Beer, A. (1852)."Bestimmung der Absorption des rothen Lichts in farbigen Flüssigkeiten", Ann. Phys. Chem 86, 78-90.
A = = exp[-μxtal(txi+ txo)
-μsolvent(tsi + tso)]
IT
Ibeam
μxtal
txi
txo
tsi
tso
txi
txo
tsi
tso
txi
txo
tsi
tso
μsolvent

## Slide 207: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 208: Darwin’s Formula
I(hkl) - photons/spot (fully-recorded)
Ibeam - incident (photons/s/m2 )
re - classical electron radius (2.818x10-15 m)
Vxtal - volume of crystal (in m3)
Vcell - volume of unit cell (in m3)
λ - x-ray wavelength (in meters!)
ω - rotation speed (radians/s)
L - Lorentz factor (speed/speed)
P - polarization factor
(1+cos2(2θ) -Pfac∙cos(2Φ)sin2(2θ))/2
A - attenuation factor
exp(-μxtal∙lpath)
F(hkl) - structure amplitude (electrons)
C. G. Darwin (1914)
P A | F(hkl) |2
I(hkl) = Ibeam re2
Vxtal
Vcell
λ3 L
ωVcell

## Slide 209: Darwin’s Formula
I(hkl) - photons/spot (fully-recorded)
Ibeam - incident (photons/s/m2 )
re - classical electron radius (2.818x10-15 m)
Vxtal - volume of crystal (in m3)
Vcell - volume of unit cell (in m3)
λ - x-ray wavelength (in meters!)
ω - rotation speed (radians/s)
L - Lorentz factor (speed/speed)
P - polarization factor
(1+cos2(2θ) -Pfac∙cos(2Φ)sin2(2θ))/2
A - attenuation factor
exp(-μxtal∙lpath)
F(hkl) - structure amplitude (electrons)
C. G. Darwin (1914)
P A | F(hkl) |2
I(hkl) = Ibeam re2
Vxtal
Vcell
λ3 L
ωVcell

## Slide 210: Lorentz Factor
Ewald sphere
Φ circle
diffracted ray
(h,k,l)
spindle axis

## Slide 211: Lorentz Factor
Ewald sphere
diffracted ray
spindle axis

## Slide 212: Lorentz Factor
Ewald sphere
diffracted ray
spindle axis

## Slide 213: Lorentz Factor
Ewald sphere
spindle axis
diffracted ray

## Slide 214: Lorentz Factor
Φ circle
diffracted ray
(h,k,l)
Ewald sphere
spindle axis

## Slide 215: Lorentz Factor
50 100 150 200 250 300 350 400 450 500
phi position (degrees)
-0.2 -0.1 0 0.1 0.2
refined mis-setting angle (degrees)

## Slide 216: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 217: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 218: Darwin’s Formula
I(hkl) - photons/spot (fully-recorded)
Ibeam - incident (photons/s/m2 )
re - classical electron radius (2.818x10-15 m)
Vxtal - volume of crystal (in m3)
Vcell - volume of unit cell (in m3)
λ - x-ray wavelength (in meters!)
ω - rotation speed (radians/s)
L - Lorentz factor (speed/speed)
P - polarization factor
(1+cos2(2θ) -Pfac∙cos(2Φ)sin2(2θ))/2
A - attenuation factor
exp(-μxtal∙lpath)
F(hkl) - structure amplitude (electrons)
C. G. Darwin (1914)
P A | F(hkl) |2
I(hkl) = Ibeam re2
Vxtal
Vcell
λ3 L
ωVcell

## Slide 219: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 220: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 221: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 222: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 223: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 224: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 225: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 226: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 227: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 228: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 229: Beam Flicker
time (seconds)
normalized flux

## Slide 230: Beam Flicker
time (seconds)
normalized flux
pinhole
removed

## Slide 231: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 232: Shutter Jitter
open
closed
shutter jitter

## Slide 233: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 234: Darwin’s Formula
I(hkl) - photons/spot (fully-recorded)
Ibeam - incident (photons/s/m2 )
re - classical electron radius (2.818x10-15 m)
Vxtal - volume of crystal (in m3)
Vcell - volume of unit cell (in m3)
λ - x-ray wavelength (in meters!)
ω - rotation speed (radians/s)
L - Lorentz factor (speed/speed)
P - polarization factor
(1+cos2(2θ) -Pfac∙cos(2Φ)sin2(2θ))/2
A - attenuation factor
exp(-μxtal∙lpath)
F(hkl) - structure amplitude (electrons)
C. G. Darwin (1914)
P A | F(hkl) |2
I(hkl) = Ibeam re2
Vxtal
Vcell
λ3 L
ωVcell

## Slide 235: xtal vibration noise
diffracted beam
incident beam

## Slide 236: xtal vibration noise
incident beam
diffracted beam

## Slide 237: xtal vibration noise
incident beam
diffracted beam

## Slide 238: xtal vibration noise
incident beam
diffracted beam

## Slide 239: xtal vibration noise
incident beam
diffracted beam

## Slide 240: xtal vibration noise
incident beam
diffracted beam

## Slide 241: Shutter Jitter
rms timing error (% exposure)
CC to correct model

## Slide 242: Beam Flicker
flicker noise (%/√Hz)
CC to correct model

## Slide 243: Solution to vibration:
attenu-wait!
reduce flux
increase exposure
Solution to systematic error:
Never use same pixel twice

## Slide 244: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 245: Detector calibration
plastic
air
fibers
Gd2O2S:Tb

## Slide 246: Detector calibration
plastic
air
fibers
Gd2O2S:Tb
x-rays

## Slide 247: Detector calibration
plastic
air
fibers
Gd2O2S:Tb
x-rays

## Slide 248: Detector calibration
plastic
air
fibers
Gd2O2S:Tb
x-rays

## Slide 249: Detector calibration
plastic
air
fibers
Gd2O2S:Tb
x-rays

## Slide 250: Detector calibration
plastic
air
fibers
Gd2O2S:Tb
x-rays

## Slide 251: Detector calibration
plastic
air
fibers
Gd2O2S:Tb
x-rays

## Slide 252: Detector calibration: 7247 eV
target:
oil
distance:
900 mm
2θ: 12°

## Slide 253: Detector calibration: 7235 eV
target:
oil
distance:
900 mm
2θ: 12°

## Slide 254: Detector calibration
-10%
+10%

## Slide 255: Detector calibration errors: detector 2

## Slide 256: Detector calibration errors: detector 3

## Slide 257: Detector calibration errors
Dan Schuette PhD Thesis (2008) Fig 6.22 page 198, Gruner Lab, Cornell University.
Pixel arrays are not immune!

## Slide 258: Spatial Noise

## Slide 259: Spatial Noise
down

## Slide 260: Spatial Noise
down
up

## Slide 261: Spatial Noise
down
up
Rseparate

## Slide 262: Spatial Noise
odd
even
Rmixed

## Slide 263: Spatial Noise
separate:
2.5%

## Slide 264: Spatial Noise
separate:
mixed:
2.5%
0.9%

## Slide 265: Spatial Noise
separate:
mixed:
2.5%
0.9%
2.5%2-0.9%2 = 2.3%2

## Slide 266: Spatial Noise: Q315r vs Pilatus
Holton, Frankel, Gonzalez, Waterman and Wang (2010) in preparation
3.5
3.0
2.5
2.0
1.5
1.0
0.5
average change in spot intensity (%)
distance between spots (mm)
0.1 1 10 100
Pilatus
Q315r
anomalous mates typically
> 100 mm apart

## Slide 267: Required multiplicity
mult > (—)2
~3%
<ΔF/F>

## Slide 268: Multi-crystal strategies
Kendrew et al. (1960) "Structure of Myoglobin” Nature 185, 422-427.

## Slide 269: 140-fold multiplicity 16 crystals
7.4σ = Na
DELFAN residual anomalous difference
data Courtesy of Tom & Janet

## Slide 270: Discerning Na+ from Mg++
f’’ (electrons)
DELFAN peak height (σ)
Mg
Ne
Na
F
O
N

## Slide 271: Detector calibration
photon energy (keV)
calibration error (%)
good!
good!
bad!

## Slide 272
7247 eV

## Slide 273
7235 eV

## Slide 274: Detector calibration
7223 eV

## Slide 275
Holton & Frankel (2010) Acta D 66 393-408.

## Slide 276: What is holding us back?
Weak spots (high-res)
  background
  solution: use as few pixels as possible
MAD/SAD (small differences)
  fractional errors
  solution: use as many pixels as possible
( if not rad dam! )

## Slide 277: Summary
100 ADU/pixel
10 MGy/Å
~3% error per spot, 1%/MGy
7235 eV for S-SAD
http://bl831.als.lbl.gov/xtalsize.html
http://bl831.als.lbl.gov/~jamesh/powerpoint/AACS_diffraction_2013.pptx