## Slide 1: Diffraction
When “scattering”
is not random

## Slide 2
detector
sample
detector
x-ray beam
scattering

## Slide 4: Scattering: atom by atom
h index
intensity

## Slide 5: Scattering: atom by atom
h index
intensity

## Slide 6
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 7
scattering from a lattice
colored by phase
sample
detector

## Slide 8
scattering from a molecule
colored by phase
sample
detector

## Slide 9
scattering from a crystal structure
colored by phase
sample
detector

## Slide 10: Spot shape
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*

## Slide 11: mosaic spread
Ewald sphere
spindle axis
Φ circle
diffracted rays
(h,k,l)
d*
d*

## Slide 12: mosaic spread = 12.8º

## Slide 13: beam divergence
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
Ewald sphere
λ*
λ*

## Slide 14: spectral dispersion
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ’*
λ’*

## Slide 15: dispersion = 5.1%

## Slide 16: spot shape
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ’*
λ’*
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
Ewald sphere
λ*
λ*
Ewald sphere
spindle axis
Φ circle
diffracted rays
(h,k,l)
d*
d*

## Slide 17: Now What?
10 Å

## Slide 18: Resolution
http://bl831.als.lbl.gov/~jamesh/movies/resolution.mpeg

## Slide 19: What is “disorder”?
order
order
disorder
B-factor

## Slide 20: “B” factors
ATOM 122 N LEU A 13 -3.244 25.808 19.998 1.00 16.96 N
ATOM 123 CA LEU A 13 -2.877 25.448 21.355 1.00 15.29 C
ATOM 124 C LEU A 13 -2.792 23.966 21.561 1.00 17.54 C
ATOM 125 O LEU A 13 -1.814 23.493 22.143 1.00 16.35 O
ATOM 126 CB LEU A 13 -3.907 26.164 22.268 1.00 18.72 C
ATOM 127 CG LEU A 13 -3.577 25.982 23.738 1.00 21.19 C
ATOM 128 CD1 LEU A 13 -2.283 26.820 24.019 1.00 19.43 C
ATOM 129 CD2 LEU A 13 -4.702 26.474 24.639 1.00 24.65 C
ATOM 130 N SER A 14 -3.677 23.149 20.979 1.00 15.96 N
ATOM 131 CA SER A 14 -3.646 21.711 21.061 1.00 18.26 C
ATOM 132 C SER A 14 -2.373 21.203 20.360 1.00 18.71 C
ATOM 133 O SER A 14 -1.747 20.315 20.930 1.00 17.47 O
ATOM 134 CB SER A 14 -4.875 21.077 20.419 1.00 17.62 C
ATOM 135 OG ASER A 14 -4.825 19.665 20.388 0.50 20.89 O
ATOM 136 OG BSER A 14 -6.027 21.408 21.164 0.50 18.67 O
ATOM 137 N LYS A 15 -2.045 21.772 19.215 1.00 18.03 N
ATOM 138 CA LYS A 15 -0.799 21.361 18.555 1.00 18.12 C
ATOM 139 C LYS A 15 0.446 21.707 19.351 1.00 18.81 C
ATOM 140 O LYS A 15 1.400 20.948 19.411 1.00 17.77 O
ATOM 141 CB LYS A 15 -0.700 22.034 17.177 1.00 14.49 C
ATOM 142 CG LYS A 15 -1.727 21.368 16.256 1.00 16.12 C
ATOM 143 CD LYS A 15 -1.663 22.147 14.936 1.00 19.40 C
ATOM 144 CE ALYS A 15 -2.725 21.614 13.986 0.50 17.42 C
ATOM 145 CE BLYS A 15 -1.750 21.211 13.750 0.50 17.01 C
ATOM 146 NZ ALYS A 15 -2.346 21.674 12.559 0.50 18.61 N
ATOM 147 NZ BLYS A 15 -3.052 20.513 13.741 0.50 18.76 N

## Slide 21: “B” factors
B = 8π2 ux2
ux = RMS variation perpendicular to plane

## Slide 22
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 23: “B” factors
B ≈ 4d2 + 12
essentially, the “resolution” of an atom
d = resolution in Å

## Slide 24: Debye-Waller-Ott factor
F - structure factor
A - something Debye said was zero
B - canonical Debye-Waller factor
C - something else Debye said was zero
s - 0.5/d
d - resolution of spot (Å)
F = F0 exp( - A∙s - B∙s2 - C∙s3 - … )

## Slide 25: Debye-Waller-Ott factor
normalized total intensity
Resolution (Ǻ)
 5 2.5 1.7 1.25 1.0
Gaussian
Exponential
Reciprocal Space

## Slide 26: Debye-Waller-Ott factor
normalized number of atoms
magnitude of displacement (Å)
Lorentzian
Gaussian
Direct Space

## Slide 27
scaled <F2>
(sin(θ)/λ)2
Wilson plot
4.1 3.5 3.2 2.9 2.7 2.5 2.4 2.2 2.1
resolution (Å)
Rcryst/Rfree
0.355/0.514
0.257/0.449
0.209/0.407

## Slide 28: Purity is crucial!
McPherson, A., Malkin, A. J., Kuznetsov, Y. G. & Plomp, M. (2001)."Atomic force microscopy applications in macromolecular crystallography", Acta Cryst. D 57, 1053-1060.
not important for
initial hits
important for
resolution

## Slide 29: What can I improve?
Purity!
is 95% good enough? 99%?
Purity!
conformational (homogeneous)
Purity!
kinetic (stable over time)

## Slide 30: What can I improve?
add a column
fractional recrystallization
heat shock
mutate Lys
avoid stress
Newman J. (2006) Acta Cryst. D62 27-31.

## Slide 31: causes of stress
physical contact
don’t touch the part you intend to shoot
osmotic shock
equilibrate, or calculate matching solution
changes in dielectric constant
Petsko (1975) J. Mol. Biol. 96, 381-388.
cooled density mismatch
Juers & Matthews (2004) Acta Cryst. D 60, 412-421.
basically: no sudden moves!

## Slide 32: Completeness: missing wedge
http://bl831.als.lbl.gov/~jamesh/movies/osc.mpeg

## Slide 33: Non-isomorphism in lysozyme
RH 84.2% vs 71.9%
Riso = 44.5%
RMSD = 0.18 Å

## Slide 34: oiled drop: you have ~3 hours
oil

## Slide 35: signal vs noise
“photon counting”
Read-out noise
Shutter jitter
Beam flicker
spot shape
radiation damage
σ(N) = sqrt(N)
rms 11.5 e-/pixel
rms 0.57 ms
0.15 %/√Hz
pixels? mosaicity?
B/Gray?

## Slide 36: signal vs noise
fractional noise
“photon counting”
constant noise
σ(I) = k x I “% error”
σ(I) = k x sqrt(I)
σ(I) = k

## Slide 37: Optimal exposure time (faint spots)
thr Optimal exposure time for data set (s)
tref exposure time of reference image (s)
bgref background level near weak spots on
reference image (ADU)
bg0 ADC offset of detector (ADU)
bghr optimal background level (via thr)
σ0 rms read-out noise (ADU)
gain ADU/photon
m multiplicity of data set (including partials)
adjust exposure
so this is ~100

## Slide 38
sample
detector
x-ray beam
anomalous scattering

## Slide 39
anomalous signal
Crick, F. H. C. & Magdoff, B. S. (1956) Acta Crystallogr. 9, 901-908.
Hendrickson, W. A. & Teeter, M. M. (1981) Nature 290, 107-113.
# sites
MW (Da)
ΔF
F
≈ 1.2 f”
√
f” | Element
0.5 | S P
4 | Se Br Fe
10 | Hg Gd Au Pt
World record!
ΔF/F = 0.5%
Wang, Dauter & Dauter (2006) Acta Cryst. D 62, 1475-1483.

## Slide 40: Fractional error
no “scale factor” is perfectly known
no source of light is perfectly stable
no shutter is perfectly reproducible
no crystal is perfectly still
no detector is perfectly calibrated

## Slide 41: Darwin’s Formula
I(hkl) - photons/spot (fully-recorded)
Ibeam - incident (photons/s/m2 )
re - classical electron radius (2.818x10-15 m)
Vxtal - volume of crystal (in m3)
Vcell - volume of unit cell (in m3)
λ - x-ray wavelength (in meters!)
ω - rotation speed (radians/s)
L - Lorentz factor (speed/speed)
P - polarization factor
(1+cos2(2θ) -Pfac∙cos(2Φ)sin2(2θ))/2
A - attenuation factor
exp(-μxtal∙lpath)
F(hkl) - structure amplitude (electrons)
C. G. Darwin (1914)
P A | F(hkl) |2
I(hkl) = Ibeam re2
Vxtal
Vcell
λ3 L
ωVcell

## Slide 42: attenuation factor
Bouguer, P. (1729). Essai d'optique sur la gradation de la lumière.
Lambert, J. H. (1760). Photometria: sive De mensura et gradibus luminis, colorum et umbrae. E. Klett.
Beer, A. (1852)."Bestimmung der Absorption des rothen Lichts in farbigen Flüssigkeiten", Ann. Phys. Chem 86, 78-90.
A = = exp[-μxtal(txi+ txo)
-μsolvent(tsi + tso)]
IT
Ibeam
μxtal
txi
txo
tsi
tso
txi
txo
tsi
tso
txi
txo
tsi
tso
μsolvent

## Slide 43: Lorentz Factor
Φ circle
diffracted ray
(h,k,l)
Ewald sphere
spindle axis

## Slide 44: % error from rad dam
Riso (%)
change in dose (MGy)
data taken from Banumathi, et al. (2004) Acta Cryst. D 60, 1085-1093.
Riso ≈ 0.7 %/MGy

## Slide 45: Beam Flicker
1/f noise or “flicker noise”
comes from everything

## Slide 46: Shutter Jitter
open
closed
shutter jitter

## Slide 47: xtal vibration noise
incident beam
diffracted beam

## Slide 48: Shutter Jitter
rms timing error (% exposure)
CC to correct model

## Slide 49: Beam Flicker
flicker noise (%/√Hz)
CC to correct model

## Slide 50: Solution to vibration:
attenu-wait!
reduce flux
increase exposure

## Slide 51: Detector calibration
plastic
air
fibers
Gd2O2S:Tb
x-rays

## Slide 52: Spatial Noise
down
up
Rseparate

## Slide 53: Spatial Noise
separate:
mixed:
2.5%
0.9%
2.5%2-0.9%2 = 2.3%2

## Slide 54: Required multiplicity
mult > (—)2
~3%
<ΔF/F>

## Slide 55: 140-fold multiplicity
7.4σ = Na
DELFAN residual anomalous difference
data Courtesy of Tom & Janet

## Slide 56: Detector calibration
photon energy (keV)
calibration error (%)
good!
good!
bad!

## Slide 57
Holton & Frankel (2010) Acta D 66 393-408.

## Slide 58: What is holding us back?
Weak spots (high-res)
  background
  solution: use as few pixels as possible
MAD/SAD (small differences)
  fractional errors
  solution: use as many pixels as possible
( if not rad dam! )

## Slide 59: Summary
100 ADU/pixel
10 μm for lysozyme
~3% error per spot, 1%/MGy
7235 eV for S-SAD
http://bl831.als.lbl.gov/xtalsize.html
http://bl831.als.lbl.gov/~jamesh/mlfsom/
http://bl831.als.lbl.gov/~jamesh/powerpoint/AACS_diffraction_2013.ppt