## Slide 1: Acknowledgements
UCSF LBNL SLAC
ALS 8.3.1: TomAlberTron
UC Multicampus Research Programs and Initiatives (MRPI)
NIH NIGMS R01 GM124149
NIH NIGMS P30 GM124169
Integrated Diffraction Analysis Technologies (IDAT)
Plexxikon, Inc.
Synchrotron Radiation Structural Biology Resource (SLAC)
The Advanced Light Source is supported by the Director, Office of Science, Office of Basic Energy Sciences, Materials Sciences Division, of the US Department of Energy under contract No. DE-AC02-05CH11231 at Lawrence Berkeley National Laboratory.
Robert Stroud James Fraser John Spence
Chris Nielsen Clemens Schulze-Briese Aina Cohen Ana Gonzalez

## Slide 2: PowerPoint File available:
http://bl831.als.lbl.gov/
~jamesh/powerpoint/
CSHL_raddam_2018.pptx

## Slide 3: Radiation damage

## Slide 4: Where do photons go?
beamstop
Transmitted (98%)
Protein
1A x-rays

## Slide 5: Elastic scattering

## Slide 6: Elastic scattering

## Slide 7: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
Protein
1A x-rays

## Slide 8: Elastic scattering

## Slide 9: Inelastic scattering

## Slide 10: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
Protein
1A x-rays

## Slide 11: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Protein
1A x-rays

## Slide 12: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Protein
1A x-rays
Re-emitted (99%)
Absorbed (~0%)

## Slide 13: Photoelectric absorption

## Slide 14: Photoelectric absorption
e-
+

## Slide 15: Secondary ionization
e-

## Slide 16: Secondary ionization
e-
e-
+

## Slide 17: Excitation
e-

## Slide 18: Excitation
e-

## Slide 19: Excitation
e-

## Slide 20: Excitation

## Slide 21: Electron attachment
e-

## Slide 22: Electron attachment
-

## Slide 23: Sample atoms

## Slide 24: Sample atoms

## Slide 25: Primary ionization
e-
+

## Slide 26: Secondary ionizations
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+

## Slide 27: Ionization track
e-
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
+
e-
+

## Slide 28: Ionization track
e-
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
+
e-
+

## Slide 29: Ionization track

## Slide 30: Ionization track

## Slide 31: Ionization track
3 μm

## Slide 32: Ionization track
Linear Energy Transfer

## Slide 33: initial effects
e-
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
+
e-
+

## Slide 34: initial effects
e-
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
+
neutralization
e-
+

## Slide 35: initial effects
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
neutralization
e-
+

## Slide 36: initial effects
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
neutralization
neutralization
+

## Slide 37: initial effects
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
attachment
+

## Slide 38: initial effects
e-
e-
e-
e-
-
e-
e-
+
+
+
+
+
+
attachment
+

## Slide 39: initial effects
e-
e-
e-
e-
-
e-
e-
+
+
+
+
+
+
attachment
attachment
+

## Slide 40: initial effects
e-
e-
-
e-
e-
+
+
+
+
+
+
-
-
+

## Slide 41: initial effects
-
e-
+
+
+
+
+
-
-
-
-
+

## Slide 42: initial effects
-
e-
+
+
+
+
+
-
-
-
-
+
solvation

## Slide 43: initial effects
-
e-
+
+
+
+
+
-
-
-
-
solvation
+

## Slide 44: Solvated electron
e-

## Slide 45: Solvated electron
e-

## Slide 48: initial effects
-
e-
+
+
+
+
+
-
-
-
-
+

## Slide 49: initial effects
-
e-
+
+
+
+
+
-
-
-
-
+

## Slide 50: initial effects
-
e-
+
+
+
+
-
-
-
+

## Slide 51: initial effects
-
e-
+
+
-
+

## Slide 52: initial effects
-
e-
+
+

## Slide 53: Excitation transfer

## Slide 54: Excitation transfer
UV photon

## Slide 55: Excitation transfer

## Slide 56: Excitation transfer
Förster transfer
r-6

## Slide 57: Excitation transfer

## Slide 58: t = 0 s

## Slide 59: t ≈ 10-14 s
-
e-
+
+

## Slide 60: Timescales of radiation damage
Garret et. al. (2005) Chem. Rev. 105, 355-389

## Slide 61: Timescales of radiation damage
Garret et. al. (2005) Chem. Rev. 105, 355-389
LCLS
ALS
bunch

## Slide 62: Ionization track
Heterogeneous reactions
Homogeneous reactions

## Slide 63: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Protein
1A x-rays
Re-emitted (99%)
Absorbed (~0%)

## Slide 64: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Photoelectric (87%)
Protein
1A x-rays
Re-emitted (99%)
Absorbed (~0%)

## Slide 65: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
inelastic scattering (7%)
Photoelectric (87%)
Protein
1A x-rays
Re-emitted (~0%)
Absorbed (99%)
Re-emitted (99%)
Absorbed (~0%)

## Slide 66: Where do photons go?
beamstop
elastic scattering (6%)
Transmitted (98%)
useful/absorbed energy: 7.3%
inelastic scattering (7%)
Photoelectric (87%)
Protein
1A x-rays
Re-emitted (~0%)
Absorbed (99%)
Re-emitted (99%)
Absorbed (~0%)

## Slide 67: Types of radiation damage
Global
Specific

## Slide 68: Types of radiation damage
Global
Specific
  depends on chemistry

## Slide 69: Specific damage
final, refined phases

## Slide 70: Specific damage
experimentally-obtained phases

## Slide 71: Types of radiation damage
Global
Specific
  depends on chemistry
  destroys phasing signal

## Slide 72
Holton, J. M. (2007) J. Synch. Rad. 14, 51-72.

## Slide 73
1.0
0.0
fraction
unconverted
Holton, J. M. (2007) J. Synch. Rad. 14, 51-72.

## Slide 74
Holton (2009) J. Synchrotron Rad. 16 133-42
Radiation Damage World Records
MGy reaction reference
~45 global damage Owen et al. (2006)
10/Å global damage Howells et al. (2009)
5 Se-Met Holton (2007)
4 Hg-S Ramagopal et al. (2004)
4 R-C-COOH Garman et al. (2015)
3 S-S Murray et al. (2002)
1 Br-RNA Olieric et al. (2007)
~1? Cl-C ???
0.5 Mn in PS II Yano et al. (2005)
0.06 putidaredoxin Corbett et al. (2007)
0.02 Fe in myoglobin Denisov et al. (2007)

## Slide 75
Global damage
Howells, et al. (2009) J. Electron Spectrosc. Relat. Phenom. 170, 4-12.

## Slide 76: resolution dependence of global damage
resolution (Å)
maximum tolerable dose (MGy)
1 2 3 5 7 10 20 40 70 100
1
10
100
103
Howells et al. (2009) J. Electron. Spectrosc. Relat. Phenom. 170 4-12

## Slide 77: resolution dependence of global damage
resolution (Å)
maximum tolerable dose (MGy)
1 2 3 5 7 10 20 40 70 100
1
10
100
103
Howells et al. (2009) J. Electron. Spectrosc. Relat. Phenom. 170 4-12
10 MGy/Å

## Slide 78: what the is a MGy?
http://bl831.als.lbl.gov/
damage_rates.pdf
Holton J. M. (2009) J. Synchrotron Rad. 16 133-42
1 MGy = 106 J/kg

## Slide 79
How long will my crystal last?
synch line type flux beamsize flux density dose max xtal min site
ph/s μm ph/μm2/s rate lifetime lifetime
APS 5ID-B POWDER 5e12 1000x300 1.7e+07 8.25 kGy/s 61 m 4 m
APS 8-BM MAD 1e11 200 2.5e+06 858 Gy/s 9.7 h 39 m
APS 14-BM-C MONO 6e11 130x200 2.3e+07 11 kGy/s 46 m 3 m
APS 14-ID-B LAUE 7e13 15x20 2.3e+11 132 MGy/s 0.23 s 0.015 s
APS 17-BM POWDER 8e11 200 2.0e+07 8.72 kGy/s 57 m 3.8 m
APS 17-ID MAD 7e11 200 1.8e+07 9.87 kGy/s 51 m 3.4 m
APS 18-ID SAXS 2e13 50x150 2.7e+09 2.69 MGy/s 11 s 0.74 s
APS 19-BM MAD 6e+08 60x50 2.0e+05 77.3 Gy/s 4.5 d 7.2 h
APS 19-ID MAD 3e+10 100x20 1.5e+07 7.81 kGy/s 64 m 4.3 m
APS 21-ID-D MAD 5e12 50 2.0e+09 1.13 MGy/s 27 s 1.8 s
APS 21-ID-F MONO 1e12 50 4.0e+08 190 kGy/s 2.6 m 11 s
APS 21-ID-G MONO 1e12 50 4.0e+08 190 kGy/s 2.6 m 11 s
APS 22-BM MAD 7e12 40x80 2.2e+09 750 kGy/s 40 s 2.7 s
APS 22-ID MAD 7e12 40x80 2.2e+09 750 kGy/s 40 s 2.7 s
APS 23-BM-B MAD 2e11 200? 5.0e+06 2.47 kGy/s 3.4 h 13 m
APS 23-ID-B MAD 6e12 80x20 3.8e+09 2.11 MGy/s 14 s 0.95 s
APS 23-ID-D MAD 1e13 75x25 5.3e+09 3.01 MGy/s 10 s 0.66 s
APS 24-ID-C MAD 2.5e12 40x60 1.0e+09 357 kGy/s 84 s 5.6 s
APS 24-ID-E MONO 2.85e12 20x120 1.2e+09 563 kGy/s 53 s 3.5 s
APS 31-ID MAD 2.6e12 120x80 2.7e+08 105 kGy/s 4.8 m 19 s
NSLS-II 17-ID-1 MAD 5e12 7x5 1.4e+11 67 MGy/s 0.45 s 0.03 s
NSLS-II 17-ID-2 MAD 2e12 1x1 1.3e+12 626 MGy/s 0.048 s 0.0032 s
NSLS X3A MAD 3.8e10 200 9.5e+05 451 Gy/s 18 h 74 m
NSLS X3B EXAFS 9e11 200x700 6.4e+06 6.48 kGy/s 77 m 5.1 m
NSLS X4A MAD 2e10 300 2.2e+05 136 Gy/s 61 h 4.1 h
NSLS X6A MAD 1.5e12 100x500 3.0e+07 10.3 kGy/s 49 m 3.2 m
NSLS X8C MAD 1.1e10 200? 2.8e+05 204 Gy/s 41 h 2.7 h

## Slide 80: Life-halving concentration
Na | 44
Mg | 27
P | 9
S | 7
Cl | 5
K | 3.3
Ca | 2.7
Fe | 1.0
Cu | 0.67
Zn | 0.58
molar, at the Se edge based on RADDOSE
As | 0.44
Se | 0.42
Br | 2.9
I | 0.47
Gd | 0.21
Ta | 0.13
Pt | 0.17
Au | 0.16
Hg | 0.16
U | 0.23

## Slide 81: Life-halving concentration
Na | 44
Mg | 27
P | 9
S | 7
Cl | 5
K | 3.3
Ca | 2.7
Fe | 1.0
Cu | 0.67
Zn | 0.58
molar, at the Se edge based on RADDOSE
As | 0.44
Se | 0.42
Br | 2.9
I | 0.47
Gd | 0.21
Ta | 0.13
Pt | 0.17
Au | 0.16
Hg | 0.16
U | 0.23

## Slide 82
660%

## Slide 83: Can radiation damage be prevented?
Yes! By keeping dose low

## Slide 85
Holton & Frankel (2010) Acta D 66 393-408.

## Slide 86: Multi-crystal strategies
Kendrew et al. (1960) "Structure of Myoglobin” Nature 185, 422-427.

## Slide 87: Can radiation damage be “outrun”?

## Slide 88: Dose-rate dependence of damage
dose rate (kGy/s)
maximum useful dose (MGy)

## Slide 89: Dose-rate effect at Room Temp?
Warkentin M, Badeau R, Hopkins JB, Mulichak AM, Keefe LJ & Thorne RE (2012)."Global radiation damage at 300 and 260 K with dose rates approaching 1 MGy s-1", Acta Cryst. D 68, 124-133.
Owen RL, Axford D, Nettleship JE, Owens RJ, Robinson JI, Morgan AW, Dore AS, Lebon G, Tate CG, Fry EE, Ren J, Stuart DI & Evans G (2012)."Outrunning free radicals in room-temperature macromolecular crystallography", Acta Cryst. D 68, 810-818.

## Slide 90: Gaussian beam
50% of flux
the other 50%

## Slide 91: Collimated beam
100% of flux
0%

## Slide 92: Tipping point for µfocus:
10 µm
~10 mm
~1 mrad =0.06°

## Slide 93: No Damage in the Dark!
Experiment time (hours)
Peak absorbance (electrons)
4.6 5.0 5.4 5.8 6.2 6.6
0 5 10 15 20 25

## Slide 94: Double-tap: no dark progression at 675 kGy/s
Intensity (photons)
Time (seconds)

## Slide 95: Xtal5_t1 graph

## Slide 96: How much water are we burning?
Meents et al. (2010) claimed:
"400 molecules of H2 for every 12.5 keV photon“
= 3.3x10-7 mol/J
200 kGy to 100 um3 = 0.24 J
= 1.2x10-8 mol H2
100 um3 of water = 6.7x10-8 mol
→ 18% of water has reacted!

## Slide 97: thaw
Radiation damage

## Slide 98: Can radiation damage be “outrun”?
not really

## Slide 99
Where:
IDL - average damage-limited intensity (photons/hkl) at a given resolution
105 - converting R from μm to m, re from m to Å, ρ from g/cm3 to kg/m3 and MGy to Gy
re - classical electron radius (2.818 x 10-15 m/electron)
h - Planck’s constant (6.626 x 10-34 J∙s)
c - speed of light (299792458 m/s)
fdecayed - fractional progress toward completely faded spots at end of data set
ρ - density of crystal (~1.2 g/cm3)
R - radius of the spherical crystal (μm)
λ - X-ray wavelength (Å)
fNH - the Nave & Hill (2005) dose capture fraction (1 for large crystals)
nASU - number of proteins in the asymmetric unit
Mr - molecular weight of the protein (Daltons or g/mol)
VM - Matthews’s coefficient (~2.4 Å3/Dalton)
H - Howells’s criterion (10 MGy/Å)
θ - Bragg angle
a2 - number-averaged squared structure factor per protein atom (electron2)
Ma - number-averaged atomic weight of a protein atom (~7.1 Daltons)
B - average (Wilson) temperature factor (Å2)
μ - attenuation coefficient of sphere material (m-1)
μen - mass energy-absorption coefficient of sphere material (m-1)
Self-calibrated damage limit
Holton & Frankel (2010) Acta D 66 393-408.
No flux
No symmetry
No exposure time

## Slide 100
The number of photons scattered
before crystal is dead
is independent
of flux & time
1 um3 = 105 photons (roomT)
1 um3 = 106 photons (synch)
1 um3 = 108 photons (XFEL)
Henderson, 1990; Gonzalez & Nave, 1994; Glaeser et al., 2000; Sliz et al., 2003; Leiros et al., 2006; Owen et al., 2006; Garman & McSweeney, 2006; Garman & Nave, 2009; Holton, 2009
(synch)

## Slide 101: Dose slicing
crystal’s useful life
N
photons
N
photons
N
photons
unacceptable
completeness
unacceptable
read noise

## Slide 102: X-ray data are 3D!

## Slide 103: Data collection “strategy”
Dauter, Z. (1999). "Data-collection strategies." Acta Cryst. D 55(10): 1703-1717.
The “American Method”:
360° no matter what
(shoot first, questions later)

## Slide 104: Dose slicing: is that a spot?

## Slide 105: Dose slicing: is that a spot?

## Slide 106: Dose slicing: is that a spot?

## Slide 107: Dose slicing: is that a spot?

## Slide 108: Dose slicing: is that a spot?

## Slide 109: Dose slicing: is that a spot?

## Slide 110: What if?
You only have a few small crystals…
Should you:
  Collect 360° from each?
  Collect 10° from each at 36x exposure?
  Glue 36 xtals together, then collect 360° ?

## Slide 111
Chart: 
Resolution (Å)
CC vs right answer
“true” resolution limit

## Slide 112
Dose slice collection scenario |  | 
fine | coarse | glue
3.17700 | 3.14057 | 3.17604
“true” resolution vs strategy
301,640,334 photons/xtal

## Slide 113
processing procedure | resolution limit |  |  | 
 | fine | coarse | glue | glue&fine
XDS/XSCALE | 3.17700 | 3.14057 | 3.17604 | 3.12086
XDS/aimless | 3.16251 | 3.15922 | 3.16675 | 3.12162
XDS/noscale | 3.27289 | 3.15617 | 3.38929 | 3.12162
MOSFLM-defaults | x | x | x | x
MOSFLM-cheat | 3.19755 | 3.18166 | 3.20354 | 3.19755
HKL2000-defaults | x | x | x | x
HKL2000-expert | 3.21803 | 3.12646 | 3.11551 | 3.21803
HKL2000-cheat | 3.16119 | 3.10338 | 3.10338 | 3.16300
DIALS-defaults | x | x | 3.42125 | x
DIALS-expert | 3.10296 | 3.09547 | 3.07653 | 3.08465
d*Trek | ? | ? | 4.34076 | ?
EVAL15 | 3.14352 | 3.10383 | 3.09936 | 3.14105
EVAL15-sadabs | 3.13920 | 3.10797 | 3.10171 | 3.13700

## Slide 114: Minimum exposure time:
~1 photon/pixel
  PAD w XDS, DIALS
~10 photon/pixel
PAD w HKL2k, MOSFLM
~30 photon/pixel
CCD detector

## Slide 115: Can radiation damage be corrected?
Yes, if you have enough information

## Slide 116: How to loose information
long exposures
  >1 photon/image = order of arrivals
Wide phi slice
  sum over angle
Large beams
  sum over area
Pink/divergent beam
  sum over lambda/angle
Background
  non-crystal stuff
Systematics
  Dose contrast

## Slide 117: The Entropy Limit
= log2(Npixels) * flux * tsample * 1.2x10-5
minimum data rate with no information loss
Npixels = 4150*4371 for Eiger
flux = photons/s onto the sample
tsample = sample thickness in µm
1.2x10-5 = 10-4 cm/µm * cross section of oxygen (0.2 cm2/g)
* density of protein crystal (1.2 g/cm3 )
* ~1/2 of total scattering intersects detector
E.G. 34 GByte/s for 1013 photons/s and 100 µm thick
bits
s

## Slide 118: Zero-dose extrapolation (ZDE)
Diederichs, K. (2006). "Some aspects of quantitative analysis and correction of radiation damage." Acta Cryst. D 62(1): 96-101.

## Slide 119: Optimal exposure time
Dose of dataset (MGy) <= half-reaction point

## Slide 120: Types of radiation damage
Global
  scale factor
  B factor
  non-isomorphism
Specific
  depends on chemistry
  destroys phasing signal

## Slide 121: What is “disorder”?

## Slide 122: What is “disorder”?

## Slide 123: What is “disorder”?

## Slide 124: What is “disorder”?
order
order
disorder
B-factor

## Slide 125: “B” factors
ATOM 122 N LEU A 13 -3.244 25.808 19.998 1.00 16.96 N
ATOM 123 CA LEU A 13 -2.877 25.448 21.355 1.00 15.29 C
ATOM 124 C LEU A 13 -2.792 23.966 21.561 1.00 17.54 C
ATOM 125 O LEU A 13 -1.814 23.493 22.143 1.00 16.35 O
ATOM 126 CB LEU A 13 -3.907 26.164 22.268 1.00 18.72 C
ATOM 127 CG LEU A 13 -3.577 25.982 23.738 1.00 21.19 C
ATOM 128 CD1 LEU A 13 -2.283 26.820 24.019 1.00 19.43 C
ATOM 129 CD2 LEU A 13 -4.702 26.474 24.639 1.00 24.65 C
ATOM 130 N SER A 14 -3.677 23.149 20.979 1.00 15.96 N
ATOM 131 CA SER A 14 -3.646 21.711 21.061 1.00 18.26 C
ATOM 132 C SER A 14 -2.373 21.203 20.360 1.00 18.71 C
ATOM 133 O SER A 14 -1.747 20.315 20.930 1.00 17.47 O
ATOM 134 CB SER A 14 -4.875 21.077 20.419 1.00 17.62 C
ATOM 135 OG ASER A 14 -4.825 19.665 20.388 0.50 20.89 O
ATOM 136 OG BSER A 14 -6.027 21.408 21.164 0.50 18.67 O
ATOM 137 N LYS A 15 -2.045 21.772 19.215 1.00 18.03 N
ATOM 138 CA LYS A 15 -0.799 21.361 18.555 1.00 18.12 C
ATOM 139 C LYS A 15 0.446 21.707 19.351 1.00 18.81 C
ATOM 140 O LYS A 15 1.400 20.948 19.411 1.00 17.77 O
ATOM 141 CB LYS A 15 -0.700 22.034 17.177 1.00 14.49 C
ATOM 142 CG LYS A 15 -1.727 21.368 16.256 1.00 16.12 C
ATOM 143 CD LYS A 15 -1.663 22.147 14.936 1.00 19.40 C
ATOM 144 CE ALYS A 15 -2.725 21.614 13.986 0.50 17.42 C
ATOM 145 CE BLYS A 15 -1.750 21.211 13.750 0.50 17.01 C
ATOM 146 NZ ALYS A 15 -2.346 21.674 12.559 0.50 18.61 N
ATOM 147 NZ BLYS A 15 -3.052 20.513 13.741 0.50 18.76 N

## Slide 126: The B factor
Bragg, W. H. (1914)."XCVII. The intensity of reflexion of X rays by crystals", Philosophical Magazine Series 6 27, 881-899. Published May 1 1914

## Slide 127: B factor from image analysis
B = 500

## Slide 128: B factor from image analysis
B = 20

## Slide 129
Crystal diameter (micron)
Resolution (Å)
B = 0
B = 20
B = 60
B = 170
B = 330
B = 560
B = 850
Bigger is better, but not by much

## Slide 130
disorder
+ averaging
= poor resolution
Diffraction Take-Home Lesson:

## Slide 131: What Causes Disorder?
Function
Radiation damage
Mosaicity
Strain
Xtal abuse
Dehydration

## Slide 132: What Causes Disorder?
Function
Radiation damage
Mosaicity
Strain
Xtal abuse
Dehydration

## Slide 133: Muybridge’s galloping horse (1878)

## Slide 134: realistic “crystal” of horses

## Slide 135: average structure: galloping horse

## Slide 136: Ways to improve order
New crystal form
Purify
  - add a column
  - heat shock
Bind something
  - Known ligand
  - Silver bullets
Change the clone
  - chop off floppy bits
  - homolog
  - Ala -> Lys mutants
Make Protein Sit Still!!!
Newman J. (2006) Acta Cryst. D62 27-31.
8000 cases in PDB of resolution improvement
80% of these are different crystal forms
> 1 Å improvement → 94% different forms

## Slide 137: What Causes Disorder?
Function
Radiation damage
Mosaicity
Strain
Xtal abuse
Dehydration

## Slide 138: not enough signal

## Slide 139: brighter light

## Slide 140: even brighter

## Slide 141: very bright light

## Slide 142: Correct structure

## Slide 143: Types of radiation damage
Global
  scale factor
  B factor
  non-isomorphism
Specific
  depends on chemistry
  destroys phasing signal

## Slide 144: Riso vs dose
Riso (%)
change in dose (MGy)
data taken from Banumathi, et al. (2004) Acta Cryst. D 60, 1085-1093.

## Slide 145: Riso vs dose
Riso (%)
change in dose (MGy)
data taken from Banumathi, et al. (2004) Acta Cryst. D 60, 1085-1093.
Riso ≈ 0.7 %/MGy

## Slide 146
anomalous signal
Crick, F. H. C. & Magdoff, B. S. (1956) Acta Crystallogr. 9, 901-908.
Hendrickson, W. A. & Teeter, M. M. (1981) Nature 290, 107-113.
# sites
MW (Da)
ΔF
F
≈ 1.2 f”
√
World record!
ΔF/F = 0.5%
Wang, Dauter & Dauter (2006) Acta Cryst. D 62, 1475-1483.

## Slide 147: Optimal exposure time
Dose of dataset (MGy) <= anomalous signal (%)

## Slide 148: First diffraction from protein xtal
Bernal, J. & Crowfoot, D. (1934). "X-ray photographs of crystalline pepsin", Nature 133, 794-795.
1934

## Slide 149: Dehydration: 1934
100 μm
2 mm
= 1.5 μL
= 1.0 nL
10 μm
= 1.0 pL
and 2017?
1 μm
= 1.0 fL

## Slide 150
Dear James
The story of the two forms of lysozyme crystals goes back to about 1964 when it was found that the diffraction patterns from different crystals could be placed in one of two classes depending on their intensities. This discovery was a big set back at the time and I can remember a lecture title being changed from the 'The structure of lysozyme' to 'The structure of lysozyme two steps forward and one step back'. Thereafter the crystals were screened based on intensities of the (11,11,l) rows to distinguish them (e.g. 11,11,4 > 11,11,5 in one form and vice versa in another). Data were collected only for those that fulfilled the Type II criteria. (These reflections were easy to measure on the linear diffractometer because crystals were mounted to rotate about the diagonal axis). As I recall both Type I and Type II could be found in the same crystallisation batch . Although sometimes the external morphology allowed recognition this was not infallible.
The structure was based on Type II crystals. Later a graduate student Helen Handoll examined Type I. The work, which was in the early days and before refinement programmes, seemed to suggest that the differences lay in the arrangement of water or chloride molecules (Lysozyme was crystallised from NaCl). But the work was never written up. Keith Wilson at one stage was following this up as lysozyme was being used to test data collection strategies but I do not know the outcome.
An account of this is given in International Table Volume F (Rossmann and Arnold edited 2001) p760.
Tony North was much involved in sorting this out and if you wanted more info he would be the person to contact. I hope this is helpful. Do let me know if you need more.
Best wishes
Louise
Non-isomorphism in lysozyme

## Slide 151
Johnson’s ratio
Structure factor (e-)
Non-isomorphism in lysozyme

## Slide 152
Johnson’s ratio
Structure factor (e-)
Non-isomorphism in lysozyme

## Slide 154
0.5% cell change → 15%
Crick & Magdoff (1956) “theory method isomorphous replacement”, Acta Cryst. 9, 901-8.
Same structure, different cell

## Slide 155
Same structure, different cell
0.5% cell change → 15%
Crick & Magdoff (1956) “theory method isomorphous replacement”, Acta Cryst. 9, 901-8.

## Slide 156
Same cell, rotated protein
0.5° rotation → 16%
Crick & Magdoff (1956) “theory method isomorphous replacement”, Acta Cryst. 9, 901-8.

## Slide 157
Same cell, rotated protein
0.5° rotation → 16%
Crick & Magdoff (1956) “theory method isomorphous replacement”, Acta Cryst. 9, 901-8.

## Slide 158
Uniform stretch
5% change → 0%

## Slide 159
5% change → 0%
Uniform stretch

## Slide 160: Non-isomorphism in lysozyme
RH: 84.2%
vs 71.9%
Riso = 44.5%
3aw6
3aw7
Δcell = 0.7 %
RMSD = 1.70 Å
RMSD = 0.18 Å

## Slide 161: Elastic deformation = non-isomorphism

## Slide 162: Elastic deformation = non-isomorphism

## Slide 163: Plastic deformation = poor diffraction

## Slide 164: Plastic deformation = poor diffraction

## Slide 165: … but does it work for membrane proteins?
Efremov, R. G. & Sazanov, L. A. (2011)."Structure of the membrane domain of respiratory complex I", Nature 476, 414-420.
“To improve diffraction properties, crystals were slowly cooled to 4 C, placed into micro-dialysis buttons, and mother liquor was exchanged by dialysis for 0.1 M sodium acetate (pH 4.8), 0.15 M sodium tartrate (pH 5.0), 30% PEG4000, 0.1% sodium cholate and 12.5% glycerol over a period of 5 days.”
CCP4BB:
“We used it for a large membrane protein complex and diffraction improved from ~7 to 2.7 A. The crystal is fished out and put into mother liquor solution in the button, sealed with dialysis membrane and the button is then placed into about 5 mls of mother liquor with slightly higher PEG concentration. Then you just exchange outside buffer every day or so for solutions containing higher concentrations of PEG. We went from ~9 to 30 % PEG4000 in about a week. You can easily observe crystal under microscope and if it cracks - you went too far/too quickly with PEG and need to use a bit less next time. Also, this method allows you to control all other components of the dehydrating solution - we needed to decrease salt concentration at the same time as increasing PEG. You can also introduce/increase cryo-protectant concentration at the same time. With these crystals, otherwise excellent dehydration machines already mentioned did not work, possibly because the process had to be really slow.”

## Slide 166
Magdoff & Crick (1955) “Ribonuclease II. Accuracy of measurement and shrinkage”, Acta Cryst. 8, 461-8.
Crick & Magdoff (1956) “The theory of the method of isomorphous replacement for protein crystals”, Acta Cryst. 9, 901-8.

## Slide 167: Hygrostatic gradients
loop
high
water activity
low

## Slide 168: Radiation Damage
Know your dose! (MGy)
Avoid World Records
disorder dominates everything
“Attenu-wait”: dose slicing
Stay hydrated!
http://bl831.als.lbl.gov/xtalsize.html
http://bl831.als.lbl.gov/xtallife.html
http://bl831.als.lbl.gov/~jamesh/powerpoint/CSHL_raddam_2018.pptx

## Slide 169
sample
detector
x-ray beam
scattering

## Slide 170
sample
detector
x-ray beam
scattering

## Slide 171
sample
detector
x-ray beam
scattering

## Slide 172
sample
detector
x-ray beam
scattering

## Slide 173
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 174
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 175
sample
x-ray beam
anomalous scattering
detector

## Slide 176
sample
detector
x-ray beam
anomalous scattering

## Slide 177
sample
x-ray beam
anomalous scattering
detector

## Slide 178
sample
detector
x-ray beam
anomalous scattering

## Slide 179
sample
detector
x-ray beam
anomalous scattering

## Slide 180
detector
sample
detector
x-ray beam
scattering

## Slide 183
scattering from a structure
sample
detector

## Slide 184
forward Fourier Transform
inverse Fourier Transform
no phase

## Slide 185
scattering from a structure
colored by phase
sample
detector
inverse Fourier Transform

## Slide 186
scattering from a lattice
colored by phase
sample
detector

## Slide 187
scattering from a lattice
colored by phase
sample
detector

## Slide 188
scattering from a lattice
colored by phase
sample
detector

## Slide 189
scattering from a crystal structure
colored by phase
sample
detector

## Slide 190: But my reviewer says…
Rmerge in high-resolution bin is >100% !
Answer: this is expected

## Slide 191: Expected Rmerge as Iobs → 0

## Slide 192
Average value
Averaging Gaussian error
Number of samples averaged

## Slide 193
Average value
Averaging Gauss/Gauss error
Number of samples averaged

## Slide 194
Average outer-shell Rmerge
Rmerge at the resolution limit in PDB
Year

## Slide 195: Take-home lesson:
R factors are
undefined
as Iobs → 0
Report as “ – “ in outer bin

## Slide 196: Re-indexing cheat sheet
Dauter, Z. (1999). "Data-collection strategies." Acta Cryst. D 55(10): 1703-1717.

## Slide 197: CCP4: aimless log
$TABLE: Analysis against resolution, XDSdataset:
$GRAPHS:I/sigma, Mean Mn(I)/sd(Mn(I)):0|0.216023x0|137.14:2,13,14:
:Rmerge, Rfull, Rmeas, Rpim v Resolution:0|0.216023x0|1.70834:2,4,5,6,7:
:Average I, RMSdeviation and Sd:0|0.216023x0|1650.8:2,10,11,12:
:Fractional bias:0|0.216023x0|0:2,15:
$$
N 1/d^2 Dmid Rmrg Rfull Rcum Rmeas Rpim Nmeas AvI RMSdev sd I/RMS Mn(I/sd) FrcBias $$ $$
1 0.0064 12.55 0.020 0.020 0.020 0.021 0.006 13115 1651 57 42 29.2 137.1 -
2 0.0191 7.24 0.027 0.027 0.024 0.028 0.008 24753 1171 47 42 25.0 105.2 -
3 0.0318 5.61 0.038 0.038 0.029 0.040 0.012 32197 857 46 43 18.4 79.6 -
4 0.0445 4.74 0.034 0.034 0.031 0.035 0.010 37743 1212 57 53 21.4 91.2 -
5 0.0572 4.18 0.036 0.036 0.032 0.038 0.011 42642 1181 59 57 19.9 83.8 -
6 0.0699 3.78 0.049 0.049 0.036 0.052 0.015 47224 883 59 57 15.1 65.1 -
7 0.0826 3.48 0.065 0.065 0.040 0.068 0.020 51052 685 59 58 11.7 50.9 -
8 0.0953 3.24 0.096 0.096 0.045 0.100 0.029 54636 448 56 56 8.0 35.0 -
9 0.1080 3.04 0.151 0.151 0.050 0.158 0.046 58072 268 53 53 5.1 22.7 -
10 0.1207 2.88 0.229 0.229 0.056 0.240 0.070 60731 171 51 51 3.3 15.4 -
11 0.1334 2.74 0.314 0.314 0.063 0.329 0.097 63807 125 51 51 2.4 11.3 -
12 0.1461 2.62 0.406 0.406 0.070 0.425 0.125 66241 98 51 52 1.9 8.7 -
13 0.1588 2.51 0.537 0.537 0.078 0.562 0.166 68272 76 53 53 1.4 6.5 -
14 0.1715 2.41 0.685 0.685 0.084 0.727 0.237 54170 61 53 54 1.1 4.4 -
15 0.1843 2.33 0.886 0.886 0.088 0.950 0.333 39781 48 55 56 0.9 3.1 -
16 0.1970 2.25 1.249 1.249 0.092 1.355 0.508 29754 35 57 59 0.6 2.1 -

## Slide 198: CCP4: aimless log
$TABLE: Correlations CC(1/2) within dataset, XDSdataset:
$GRAPHS: Anom & Imean CCs v resolution:0|0.216023x0|1:2,4,7:
: RMS correlation ratio :0|0.216023x0|2.20344:2,6:
$$
N 1/d^2 Dmid CCanom Nanom RCRanom CC1/2 NImean $$ $$
1 0.0064 12.55 0.659 499 2.203 1.000 669
2 0.0191 7.24 0.550 975 1.853 1.000 1155
3 0.0318 5.61 0.527 1295 1.798 1.000 1479
16 0.1970 2.25 0.037 2123 1.038 0.711 2275
17 0.2097 2.18 0.043 1682 1.044 0.460 1877

## Slide 199: XDS: CORRECT.LP or XSCALE.LP
SUBSET OF INTENSITY DATA WITH SIGNAL/NOISE >= -3.0 AS FUNCTION OF RESOLUTION
RESOLUTION NUMBER OF REFLECTIONS COMPLETENESS R-FACTOR R-FACTOR COMPARED I/SIGMA R-meas CC(1/2) Anomal SigAno Nano
LIMIT OBSERVED UNIQUE POSSIBLE OF DATA observed expected Corr
6.39 4103 2517 3135 80.3% 1.7% 1.8% 3018 33.77 2.3% 99.9* 21* 1.012 533
4.54 7339 4970 5544 89.6% 2.6% 2.6% 4585 22.56 3.6% 99.8* 9 0.914 796
3.72 9442 6724 7186 93.6% 2.8% 2.9% 5327 19.99 4.0% 99.7* 9 0.859 877
3.22 11077 7997 8486 94.2% 4.8% 4.9% 6094 12.27 6.8% 99.3* -1 0.784 913
2.88 12408 8851 9595 92.2% 10.0% 10.1% 7068 6.01 14.2% 97.8* -2 0.799 1012
2.63 13673 9561 10662 89.7% 20.8% 20.8% 8185 3.10 29.4% 88.8* -4 0.776 1274
2.44 14360 9852 11510 85.6% 34.5% 34.7% 8981 1.90 48.8% 75.9* 2 0.765 1525
2.28 9501 6495 12416 52.3% 61.8% 59.6% 5991 1.14 87.3% 53.5* -2 0.722 1031
2.15 4567 3307 13210 25.0% 120.5% 120.3% 2520 0.59 170.4% 21.9* 4 0.693 408
total 86470 60274 81744 73.7% 6.7% 6.7% 51769 8.97 9.5% 99.5* 2 0.804 8369

## Slide 200: XDS: CORRECT.LP or XSCALE.LP
******************************************************************************
CORRECTION PARAMETERS FOR THE STANDARD ERROR OF REFLECTION INTENSITIES
******************************************************************************
The variance v0(I) of the intensity I obtained from counting statistics is
replaced by v(I)=a*(v0(I)+b*I^2). The model parameters a, b are chosen to
minimize the discrepancies between v(I) and the variance estimated from
sample statistics of symmetry related reflections. This model implicates
an asymptotic limit ISa=1/SQRT(a*b) for the highest I/Sigma(I) that the
experimental setup can produce (Diederichs (2010) Acta Cryst D66, 733-740).
a b ISa
3.806E+00 1.080E-04 49.32

## Slide 201: Rough values of energy quanta
1 MeV 100 GJ/mol Medical radiation therapy
100 keV 10 GJ/mol Medical imaging
10 keV 1 GJ/mol X-ray crystallography
1 keV 100 MJ/mol S and P K-edges
100 eV 10 MJ/mol “water window”
10 eV 1 MJ/mol C≡C bond
1 eV 100 kJ/mol C-C bond, visible light
100 meV 10 kJ/mol hydrogen bond
10 meV 1 kJ/mol heat (~300 K)