## Slide 1: Acknowledgements
http://bl831.als.lbl.gov/~jamesh/powerpoint/CSHL_recipspace_2022.pptx
UCSF LBNL SLAC
ALS 8.3.1: TomAlberTron
NIH NIGMS R01 GM124149 to Holton
NIH NIAID P50 AI150476 to Krogan
NIH NIAID U19 AI171110 to Krogan
NIH NIGMS P30 GM124169 to Adams
DOE-BER IDAT to Hura
NIH NIGMS P41 GM103393 to Hodgson
The Advanced Light Source is supported by the Director, Office of Science, Office of Basic Energy Sciences, Materials Sciences Division, of the US Department of Energy under contract No. DE-AC02-05CH11231 at Lawrence Berkeley National Laboratory.
Robert Stroud James Fraser
Paul Adams Greg Hura
Aina Cohen Keith Hodgson

## Slide 2: Reciprocal Space

## Slide 3: Reciprocal Space
. 1/distance
. λ = 2d sin(θ)
. Gaussian → Gaussian
. Lattice → lattice
. Duck → Blobs
Convolution → product
. Rotations same
. “angle space”
http://bl831.als.lbl.gov/~jamesh/powerpoint/CSHL_recipspace_2022.pptx

## Slide 4: X-ray data are 3D!

## Slide 5: Electric charge
-
-
-
-
-
-
+ + + + + +

## Slide 6: Electric field of a moving charge

## Slide 7: Electric field of a moving charge
accelerating charges
make
electromagnetic waves
(light)

## Slide 8
sample
detector
x-ray beam
scattering

## Slide 9
sample
detector
x-ray beam
scattering

## Slide 10
sample
detector
x-ray beam
scattering

## Slide 11
sample
detector
x-ray beam
scattering

## Slide 12
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 13
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 14
sample
x-ray beam
anomalous scattering
detector

## Slide 15
sample
detector
x-ray beam
anomalous scattering

## Slide 16
sample
x-ray beam
anomalous scattering
detector

## Slide 17
sample
detector
x-ray beam
anomalous scattering

## Slide 18
sample
detector
x-ray beam
anomalous scattering

## Slide 19
detector
sample
detector
x-ray beam
scattering

## Slide 20: nearBragg program
http://bl831.als.lbl.gov/~jamesh/nearBragg/
“assumption-free” total scattering
no Fourier Transform
no unit cells
no “mosaicity”
arbitrary “atoms”
arbitrary “source”
coherent or not

## Slide 23
scattering from a structure
sample
detector
beam center
+

## Slide 24
forward Fourier Transform
inverse Fourier Transform
no phase
+

## Slide 25
scattering from a structure
colored by phase
sample
detector
inverse Fourier Transform
+

## Slide 26
scattering from a lattice
colored by phase
sample
detector
beam center
+

## Slide 27
scattering from a lattice
colored by phase
sample
detector
beam center
+

## Slide 28
scattering from a lattice
colored by phase
sample
detector
beam center
+

## Slide 29
scattering from a crystal structure
colored by phase
sample
detector
beam center
+

## Slide 30: Muybridge’s galloping horse (1878)
Real space
reciprocal
space
“Time-resolved” diffraction
+

## Slide 31: Snapshot from single virus particle
TEM
2 keV LCLS 200 fs Mimi virus single-shot.
200 nm
Reconstructed image
Resolution 20nm
Seibert, et al. (2011). Nature 470, 78-81.
Notes: what limits single-particle resolution ?
get 100 times more photons/shot if correctly focussed beam
get 100 times more with submicron beam focus on CXI chamber
Problem – scattering goes from N^2 to N (Wilson statistics).
So use a-priori information – modelling Axel Brummer
Make beam smaller than jet to elliminate streak
31

## Slide 32: Realistic single-particle prediction
1012 photon/pulse
100 nm focus
+

## Slide 33: Realistic single-particle prediction
1012 photon/pulse
3 nm focus
+

## Slide 34: lysozyme: real and reciprocal
+
+

## Slide 35
False color intensity
sample
detector
Meaning of “Molecular Transform”
+

## Slide 36
False color intensity
sample
detector
Meaning of “Molecular Transform”
+

## Slide 37
Meaning of “Molecular Transform”
False color intensity
sample
detector
+

## Slide 38
False color intensity
sample
detector
Meaning of “Molecular Transform”
+

## Slide 39
False color intensity
sample
detector
Meaning of “Molecular Transform”

## Slide 40: Diffraction from a 3D lattice
real space
reciprocal space
+

## Slide 41: Diffraction from a 3D lattice
real space
reciprocal space
+

## Slide 42: Ewald Sphere
Ewald sphere
(h,k,l)

## Slide 43: Ewald Sphere
Ewald sphere
(h,k,l)
d*

## Slide 44: Ewald Sphere
Ewald sphere
spindle axis
(h,k,l)
d*

## Slide 45: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
(h,k,l)

## Slide 46: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
(h,k,l)

## Slide 47: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)

## Slide 48: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*

## Slide 49: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*
θ
λ = 2 d sin(θ)

## Slide 50: beam divergence
F(h,k,l)
F(0,0,0)
Ewald sphere
diffracted ray
d*
λ*
λ*

## Slide 51: beam divergence
Ewald sphere
λ*
λ*
F(0,0,0)
d*
diffracted ray

## Slide 52: Divergence Arndt & Wonacott (1977)

## Slide 53: divergence = 0 º

## Slide 54: divergence = 0.3 º

## Slide 55: spectral dispersion
Ewald sphere
diffracted ray
d*
λ*
λ*
F(h,k,l)
F(0,0,0)

## Slide 56: spectral dispersion
Ewald sphere
diffracted ray
λ’*
λ’*
F(h,k,l)
F(0,0,0)
d*

## Slide 57: dispersion = 0

## Slide 58: dispersion = 0.014% (Si 111)

## Slide 59: dispersion = 0.25% (CuKα)

## Slide 60: dispersion = 0.6%

## Slide 61: dispersion = 1.3%

## Slide 62: dispersion = 2.6%

## Slide 63: dispersion = 5.1%

## Slide 64: What if crystal is bent?

## Slide 65: What if crystal is bent?

## Slide 66: mosaic spread
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
λ*
λ*
d*
d*

## Slide 67: mosaic spread
Ewald sphere
spindle axis
Φ circle
diffracted rays
(h,k,l)
d*
d*

## Slide 68: mosaic spread = 0 º

## Slide 69: mosaic spread = 0.1º

## Slide 70: mosaic spread = 0.2º

## Slide 71: mosaic spread = 0.4º

## Slide 72: mosaic spread = 0.6º

## Slide 73: mosaic spread = 0.8º

## Slide 74: mosaic spread = 1.0º

## Slide 75: mosaic spread = 1.5º

## Slide 76: mosaic spread = 2.0º

## Slide 77: mosaic spread = 2.5º

## Slide 78: mosaic spread = 3.2º

## Slide 79: mosaic spread = 6.4º

## Slide 80: mosaic spread = 12.8º

## Slide 81: spot shape
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ’*
λ’*
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
Ewald sphere
λ*
λ*
Ewald sphere
spindle axis
Φ circle
diffracted rays
(h,k,l)
d*
d*

## Slide 82
Ewald’s “mosaic” picture

## Slide 83
Ewald’s “mosaic” picture

## Slide 84
Ewald’s “mosaic” picture
What is
this stuff?

## Slide 85
Darwin’s original picture

## Slide 86
“mosaicity” with visible light

## Slide 87
source
detector
d
atom #1
atom #2
“near”-ly Bragg’s Law

## Slide 88
“crystal”
detector
x-ray beam
peak
intensity
integrated
intensity
mosaicity vs coherence length

## Slide 89: mosaicity vs coherence length
10 atoms
0.1 μm
50 atoms
0.5 μm
100 atoms
1 μm
200 atoms
2 μm
300 atoms
3 μm
400 atoms
4 μm
500 atoms
5 μm
1000 atoms
10 μm
position on detector (mm)
intensity (photons/SR/atom)

## Slide 90: Meaning of “coherence length”
http://bl831.als.lbl.gov/~jamesh/nearBragg/collision/

## Slide 91: Meaning of “coherence length”
http://bl831.als.lbl.gov/~jamesh/nearBragg/collision/

## Slide 92: Meaning of “coherence length”
http://bl831.als.lbl.gov/~jamesh/nearBragg/collision/

## Slide 93: Meaning of “coherence length”
http://bl831.als.lbl.gov/~jamesh/nearBragg/collision/

## Slide 94: mosaicity vs coherence length
B factor
mosaic
spread
intensity (photons/SR)
number of atoms in line

## Slide 95: “B” factors
ATOM 122 N LEU A 13 -3.244 25.808 19.998 1.00 16.96 N
ATOM 123 CA LEU A 13 -2.877 25.448 21.355 1.00 15.29 C
ATOM 124 C LEU A 13 -2.792 23.966 21.561 1.00 17.54 C
ATOM 125 O LEU A 13 -1.814 23.493 22.143 1.00 16.35 O
ATOM 126 CB LEU A 13 -3.907 26.164 22.268 1.00 18.72 C
ATOM 127 CG LEU A 13 -3.577 25.982 23.738 1.00 21.19 C
ATOM 128 CD1 LEU A 13 -2.283 26.820 24.019 1.00 19.43 C
ATOM 129 CD2 LEU A 13 -4.702 26.474 24.639 1.00 24.65 C
ATOM 130 N SER A 14 -3.677 23.149 20.979 1.00 15.96 N
ATOM 131 CA SER A 14 -3.646 21.711 21.061 1.00 18.26 C
ATOM 132 C SER A 14 -2.373 21.203 20.360 1.00 18.71 C
ATOM 133 O SER A 14 -1.747 20.315 20.930 1.00 17.47 O
ATOM 134 CB SER A 14 -4.875 21.077 20.419 1.00 17.62 C
ATOM 135 OG ASER A 14 -4.825 19.665 20.388 0.50 20.89 O
ATOM 136 OG BSER A 14 -6.027 21.408 21.164 0.50 18.67 O
ATOM 137 N LYS A 15 -2.045 21.772 19.215 1.00 18.03 N
ATOM 138 CA LYS A 15 -0.799 21.361 18.555 1.00 18.12 C
ATOM 139 C LYS A 15 0.446 21.707 19.351 1.00 18.81 C
ATOM 140 O LYS A 15 1.400 20.948 19.411 1.00 17.77 O
ATOM 141 CB LYS A 15 -0.700 22.034 17.177 1.00 14.49 C
ATOM 142 CG LYS A 15 -1.727 21.368 16.256 1.00 16.12 C
ATOM 143 CD LYS A 15 -1.663 22.147 14.936 1.00 19.40 C
ATOM 144 CE ALYS A 15 -2.725 21.614 13.986 0.50 17.42 C
ATOM 145 CE BLYS A 15 -1.750 21.211 13.750 0.50 17.01 C
ATOM 146 NZ ALYS A 15 -2.346 21.674 12.559 0.50 18.61 N
ATOM 147 NZ BLYS A 15 -3.052 20.513 13.741 0.50 18.76 N

## Slide 96: strong reflection

## Slide 97: weak reflection

## Slide 98: What is a "B factor"?

## Slide 99: What is a "B factor"?

## Slide 100: What is a "B factor"?

## Slide 101: What is a "B factor"?
order
order
disorder
B-factor

## Slide 102
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 103
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 104
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 105
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 106
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 107
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 108
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 109
electron density (e-/Å3)
position (Å)
“B” factors

## Slide 110: A Fourier view of scattering
distance (Å)
density (ρ)
angle (°)
intensity

## Slide 111: A Fourier view of scattering
distance (Å)
density (ρ)
angle (°)
intensity

## Slide 112: A Fourier view of scattering
distance (Å)
density (ρ)
angle (°)
intensity

## Slide 113: A Fourier view of scattering
distance (Å)
density (ρ)
angle (°)
intensity

## Slide 114: B factor from image analysis
B = 500

## Slide 115: B factor from image analysis
B = 20

## Slide 116: The B factor
Bragg, W. H. (1914)."XCVII. The intensity of reflexion of X rays by crystals", Philosophical Magazine Series 6 27, 881-899. Published May 1 1914

## Slide 117: Resolution
http://bl831.als.lbl.gov/~jamesh/movies/resolution.mpeg

## Slide 118: Resolution: low-angle cutoff
http://bl831.als.lbl.gov/~jamesh/movies/lo_cut.mpeg

## Slide 119: R-factor
http://bl831.als.lbl.gov/~jamesh/movies/rfactor.mpeg

## Slide 120: Figure of Merit
http://bl831.als.lbl.gov/~jamesh/movies/dephase.mpeg

## Slide 121: Overloads
http://bl831.als.lbl.gov/~jamesh/movies/overloads.mpeg

## Slide 122: Completeness: missing wedge
http://bl831.als.lbl.gov/~jamesh/movies/osc.mpeg

## Slide 123: Completeness: random deletion
http://bl831.als.lbl.gov/~jamesh/movies/completeness.mpeg

## Slide 124
Crystal diameter (micron)
Resolution (Å)
B = 0
B = 20
B = 60
B = 170
B = 330
B = 560
B = 850
Bigger is better, but not by much

## Slide 125
disorder
+ averaging
= poor resolution
Diffraction Take-Home Lesson:

## Slide 126: Lorentz factor: note added in proof
Debye, P. J. W. (1914)."Interferenz von Röntgenstrahlen und Wärmebewegung", Annalen der Physik 348, 49-92.
Lorentz

## Slide 127: Lorentz Factor
Ewald sphere
Φ circle
diffracted ray
(h,k,l)
spindle axis

## Slide 128: Lorentz Factor
Ewald sphere
diffracted ray
spindle axis

## Slide 129: Lorentz Factor
Ewald sphere
diffracted ray
spindle axis

## Slide 130: Lorentz Factor
Ewald sphere
spindle axis
diffracted ray

## Slide 131: The “Lorentz zone”

## Slide 132: Lorentz factor
+
50x
1.2x
550x
3x
10x

## Slide 133: Polarization factor
1.0
0.45
+

## Slide 134: attenuation factor
Bouguer, P. (1729). Essai d'optique sur la gradation de la lumière.
Lambert, J. H. (1760). Photometria: sive De mensura et gradibus luminis, colorum et umbrae. E. Klett.
Beer, A. (1852)."Bestimmung der Absorption des rothen Lichts in farbigen Flüssigkeiten", Ann. Phys. Chem 86, 78-90.
A = = exp[-μxtal(txi+ txo)
-μsolvent(tsi + tso)]
IT
Ibeam
μxtal
txi
txo
tsi
tso
txi
txo
tsi
tso
txi
txo
tsi
tso
μsolvent

## Slide 135: Where do photons go?
beamstop
98%
Transmitted
100 µm Protein
1 Å X-rays
error < total < 2%

## Slide 136: Air absorption
Distance from sample (mm)
transmittance

## Slide 137
Pick-up tool mark
Bragg
glitch
oxygen
inclusions
“tree rings”
1% high
average
1% low
~3x105 photon/pixel Pilatus detector
Spatial Heterogeneity in Sharp Spot Sensitivity

## Slide 138: A few other corrections…
Meisburger, et. al. Nat Commun 11, 1271 (2020). https://doi.org/10.1038

## Slide 139
CORRECT – after all the “factors”

## Slide 140: Reciprocal Space
. 1/distance
. λ = 2d sin(θ)
. Gaussian → Gaussian
. Lattice → lattice
. Convolution → product
. Rotations same
. “angle space”
http://bl831.als.lbl.gov/~jamesh/powerpoint/CSHL_recipspace_2022.pptx

## Slide 141: Temperature is not enough
Debye, P. J. W. (1914)."Interferenz von Röntgenstrahlen und Wärmebewegung", Annalen der Physik 348, 49-92.

## Slide 142: Dawn of the Age of Uncertainty

## Slide 143: Temperature is not enough
Debye, P. J. W. & Scherrer, P. (1918)."Atomic structure", Physikalische Zeitschrift 19, 474-483.
Scherrer
30
Debye
35

## Slide 144: 1928: the last straw for determinism
Davisson, C. J. (1928). "The diffraction of electrons by a crystal of nickel", Bell System Technical Journal, The 7, 90-105.
Davisson-Germer Experiment
Single electron interferes with itself.
Otherwise, diffraction cannot work!

## Slide 145: How to install: nearBragg
wget http://bl831.als.lbl.gov/
~jamesh/nearBragg/nearBragg.c
gcc –o nearBragg nearBragg.c –lm
./nearBragg
usage: nearBragg -file atom_list.txt
options:
-file filename.txt text file containing point scatterer coordinates in Angstrom relative to the origin.
-distance from origin to detector center in mm
-detsize detector size in mm. may also use -detsize_x -detsize_y
-detpixels detector size in pixels. may also use -detpixels_x -detpixels_y
-pixel detector pixel size in mm.

## Slide 146: How to run: nearBragg for single particle
egrep “^ATOM|^HETAT” lysozyme.pdb |\
awk ‘{print substr($0,31,36)}’ |\
cat >! atoms.txt
wget bl831.als.lbl.gov/~jamesh/nearBragg/rotate.awk
./rotate.awk -v phix=10 -v phiy=20 -v phiz=30 atoms.txt >! rotated.txt
nearBragg –atoms rotated.txt -lambda 1 -distance 1000 -detsize 100 -fluence 1e32
(200s)
adxv intimage.img

## Slide 147: How to run: nearBragg for single particle
egrep “^ATOM|^HETAT” lysozyme.pdb |\
awk ‘{print substr($0,31,36)}’ |\
cat >! atoms.txt
wget bl831.als.lbl.gov/~jamesh/nearBragg/rotate.awk
./rotate.awk -v phix=10 -v phiy=20 -v phiz=30 atoms.txt >! rotated.txt
nearBragg –atoms rotated.txt -lambda 1 -distance 1000 -detsize 100 -fluence 1e32
(200s)
adxv intimage.img

## Slide 148: How to run: nearBragg for single particle
egrep “^ATOM|^HETAT” lysozyme.pdb |\
awk ‘{print substr($0,31,36)}’ |\
cat >! atoms.txt
wget bl831.als.lbl.gov/~jamesh/nearBragg/rotate.awk
./rotate.awk -v phix=10 -v phiy=20 -v phiz=30 atoms.txt >! rotated.txt
nearBragg –atoms rotated.txt -lambda 1 -distance 1000 -detsize 100 -fluence 1e32
(200s)
adxv noiseimage.img

## Slide 149: How to run: nanoBragg for single particle
pdbset xyzin lysozyme.pdb xyzout bigcell.pdb << EOF
CELL 250 250 250 90 90 90
SPACEGROUP 1
EOF
phenix.fmodel bigcell.pdb high_resolution=10 k_sol=0.35 b_sol=46.5 mask.solvent_radius=0.5 mask.shrink_truncation_radius=0.16
mtz_to_P1hkl.com bigcell.pdb.mtz
nanoBragg –cell 250 250 250 90 90 90 –misset 10 20 30 -hkl P1.hkl -lambda 1 -distance 1000 -detsize 100 -fluence 1e32 -N 1
adxv noiseimage.img

## Slide 150: How to run: nanoBragg for single particle
pdbset xyzin lysozyme.pdb xyzout bigcell.pdb << EOF
CELL 250 250 250 90 90 90
SPACEGROUP 1
EOF
phenix.fmodel bigcell.pdb high_resolution=10 k_sol=0.35 b_sol=46.5 mask.solvent_radius=0.5 mask.shrink_truncation_radius=0.16
mtz_to_P1hkl.com bigcell.pdb.mtz
nanoBragg –cell 250 250 250 90 90 90 –misset 10 20 30 -hkl P1.hkl -lambda 1 -distance 1000 -detsize 100 -fluence 1e32 -N 1
adxv noiseimage.img

## Slide 151: How to run: nonBragg for SAXS
pdbset xyzin lysozyme.pdb xyzout bigcell.pdb << EOF
CELL 250 250 250 90 90 90
SPACEGROUP 1
EOF
phenix.fmodel bigcell.pdb high_resolution=10 k_sol=0.35 b_sol=46.5 mask.solvent_radius=0.5 mask.shrink_truncation_radius=0.16
mtz_to_stol.com bigcell.pdb.mtz
nonBragg -stol mtz.stol -lambda 1 -dispersion 0 \
-distance 1000 -detsize 100 -pixel 0.172 \
-flux 1e13 -thick 1.2 -MW 14000 -density 0.01
adxv noiseimage.img

## Slide 152: How to run: nonBragg for SAXS
pdbset xyzin lysozyme.pdb xyzout bigcell.pdb << EOF
CELL 250 250 250 90 90 90
SPACEGROUP 1
EOF
phenix.fmodel bigcell.pdb high_resolution=10 k_sol=0.35 b_sol=46.5 mask.solvent_radius=0.5 mask.shrink_truncation_radius=0.16
mtz_to_stol.com bigcell.pdb.mtz
nonBragg -stol mtz.stol -lambda 1 -dispersion 0 \
-distance 1000 -detsize 100 -pixel 0.172 \
-flux 1e13 -thick 1.2 -MW 14000 -density 0.01
adxv noiseimage.img

## Slide 153: Laue’s diffraction photograph (not to be confused with Laue diffraction)
Friedrich, W., Knipping, P. &
Laue, M. (1913). "Interferenzerscheinungen bei Röntgenstrahlen", Annalen der Physik
346, 971-988.
ZnS
Ewald, P. (1979).
"A review of my papers on crystal optics 1912 to 1968", Acta Cryst. A 35, 1-9.
Submitted
June 8 1912
“In 1910, when I began work on my thesis, there was no quantitative proof for the internal periodicity of crystals. My teacher Sommerfeld had the idea that … a lattice, would produce observable double refraction”

## Slide 154: W. L. Bragg on Spot Shape
Bragg, W. L. (1912). “On the diffraction of short electromagnetic waves by a crystal” Proc. Cambridge Philos. Soc. 17, 43-57
nλ = 2d sin θ
23 years old

## Slide 155: Reciprocal Space
. 1/distance
. λ = 2d sin(θ)
. Gaussian → Gaussian
. Lattice → lattice
. Convolution → product
. Rotations same
. “angle space”
http://bl831.als.lbl.gov/~jamesh/powerpoint/CSHL_recipspace_2022.pptx

## Slide 156: What you know when:
Autoindexing: Lattice (14)
Scaling: Point Group (43)
Phasing: Space Group (84)

## Slide 157: Asymmetric Unit (ASU)
Smallest part of the crystal
that you can use to build up the rest of the crystal
with symmetry operations
Unit Cell
Smallest part of the crystal
that you can use to build up the rest of the crystal
with translation symmetry only
“NCS ASU”
Builds ASU with Non-crystallographic symmetry operations

## Slide 158: Frequency of Space Groups in PDB
13007 | P212121 | 566 | R32 | 191 | P6322 | 74 | P4322 | 36 | P3212
9629 | P21 | 491 | P6522 | 187 | P213 | 71 | P4122 | 30 | P622
5300 | C2 | 474 | P61 | 161 | P6 | 70 | P64 | 24 | F4132
3021 | P21212 | 421 | P65 | 144 | P4212 | 70 | P6222 | 22 | P4332
2543 | C2221 | 353 | P41 | 142 | I23 | 67 | P6422 | 22 | P422
2109 | P1 | 351 | P63 | 132 | F432 | 66 | F222 | 22 | P23
2030 | P43212 | 286 | P31 | 124 | P321 | 63 | P62 | 19 | P3112
1565 | P3221 | 257 | I422 | 115 | I41 | 59 | P4132 | 18 | P4222
1359 | P41212 | 253 | P42212 | 103 | P3 | 46 | P2221 | 18 | I4132
1198 | P3121 | 249 | I4 | 99 | I213 | 43 | P4 | 16 | P432
1147 | I222 | 246 | P43 | 94 | C222 | 43 | I432 | 8 | P4232
825 | R3 | 239 | I4122 | 93 | P2 | 40 | P42 | 3 | P222
620 | P6122 | 193 | P32 | 82 | I212121 | 37 | F23 | 2 | P312

## Slide 159: Pitfalls: sub-space groups
P622
What else?
P6122 P6522 P6222 P6422 P6322
P6 P61 P65 P62 P64 P63
P312 P321 P3112 P3121 P3212 P3221
P3 P31 P32
P2 P21 C2 C222 C2221
P1
zanuda

## Slide 160: Trick Question: What is the space group?
a = 63 b = 63 c = 63
α = 90 β = 90 γ = 90