## Slide 1: What is your Space Group?
the first question asked and the last to be answered

## Slide 2: International Tables, Vol A

## Slide 3: International Tables, Vol A

## Slide 4: What is your Space Group?
What is a crystal?
What is a lattice?
What is a unit cell?
What is a symmetry operator?
What is an asymmetric unit?
Pitfalls: the “screwies”, C vs P3, alternate index
How will I know?

## Slide 5: Unit cell?

## Slide 6: Where’s the unit cell?

## Slide 7
Where’s the unit cell?

## Slide 8
Where’s the unit cell?

## Slide 9
Primitive, cubic lattice

## Slide 10
Primitive, cubic lattice

## Slide 11
Primitive, cubic lattice

## Slide 12
Primitive, cubic lattice, half-way unit cell

## Slide 13
Body-centered cell

## Slide 14
Two staggered lattices

## Slide 15
Body-centered lattice

## Slide 16
Body-centered lattice

## Slide 17: Diffraction from a 3D lattice
real space
reciprocal space
+

## Slide 18: Diffraction from a 3D lattice
real space
reciprocal space
+

## Slide 19: Diffraction from a 3D lattice
real space
reciprocal space
+
+

## Slide 20: Diffraction from a 3D lattice
real space
reciprocal space
+
+

## Slide 21
Base-centered lattice

## Slide 22
Base-centered lattice

## Slide 23
Face-centered lattice

## Slide 24
Face-centered lattice

## Slide 25
Face-centered lattice

## Slide 26
Face-centered lattice
Body-centered lattice

## Slide 27
Face-centered lattice
All half-way points

## Slide 28
Face-centered lattice
All half-way points

## Slide 29
cubic lattice

## Slide 30
rhombohedral lattice

## Slide 31
rhombohedral lattice

## Slide 32
Hexagonal version of rhombohedral lattice

## Slide 33
Hexagonal/triclinic lattice

## Slide 34
Hexagonal lattice

## Slide 35
6-fold screw operator (hexagonal)

## Slide 36
3-fold screw operator (trigonal)

## Slide 37
4-fold screw operator (tetragonal)

## Slide 38
2-fold screw operator

## Slide 39
2-fold screw operator: monoclinic lysozyme

## Slide 40: Only 4 kinds of rotation operators
3 4 6
2*2 2*3

## Slide 41
a few lysozyme crystal forms

## Slide 42: Only 5 kinds of centering
None Primitive
ABC Base
I Body
F Face
R Rhombo
No restrictions
at least two 90° angles
All angles 90°
Also fits:
All angles 90°

## Slide 43: Only 7 lattice systems
Triclinic
Monoclinic
Orthorhombic
Tetragonal
Hexagonal
Rhombohedral
Cubic
No restrictions
All angles 90°
angles same, a=b=c
All 90°; a = b = c
All 90°; square top
2x 90° angles
90° 90° 120°; a = b

## Slide 44: Only 14 lattice types in 3D
Lattice system
a asymmetric
m monoclinic
o orthorhombic
t tetragonal
h hexagonal
c cubic
Centering
P primitive (no centering)
C base (A,B not used)
I body (extra in middle)
F face (extra on each)
R rhombohedral
(two diagonal extras)
Bravais (1848)
www.ruppweb.com

## Slide 45: Enantiomorphic operators
31 32
41 43
61 65
62 64

## Slide 46: Systematic absences
How to interpret:
Every 2nd
21 42 63
Every 3rd
31 32
Every 4th
41 43
Every 6th
61 65

## Slide 47: Hermann-Mauguin symbol
P 1
Primitive
No centering
And that’s all
Also tells you: Bravais lattice = aP ; point group: 1
Unit cell can be anything

## Slide 48: Hermann-Mauguin symbol
P 43 21 2
Primitive
No centering
Yay!
4-fold screw
on “main”
axis
2-fold screw
on 2nd axis
2-fold
on 3rd axis
Also tells you: Bravais lattice = tP ; point group: 422
tetragonal system a == b and a & b are equivalent

## Slide 49: Hermann-Mauguin symbol
C 1 2 1
Base centered
On face opposite
c-axis
redundant
2-fold screw
on 2nd axis
redundant
Also tells you: Bravais lattice = mC ; point group: 2
Angles α & γ = 90°, β can be anything

## Slide 50: Hermann-Mauguin symbol
C2
Base centered
On face opposite
c-axis
2-fold screw
on 2nd axis
Also tells you: Bravais lattice = mC ; point group: 2
Angles α & γ = 90°, β can be anything

## Slide 51: Hermann-Mauguin symbol
F23
Face centered
2-fold
Also tells you: Bravais lattice = cF ; point group: 23
All edges same legnth, all angles α β γ = 90°
3-fold after
2-fold means
Cubic
(3-fold diagonal)

## Slide 52: What is a “point group”?
Essentially:
A point group is a space group
without all the subscripts

## Slide 53: Pitfalls: the “screwies”
P21212
P21221
P22121
P2221
P2212
P2122

## Slide 54: Pitfalls: sub-space groups
P622
What else?
P6122 P6522 P6222 P6422 P6322
P6 P61 P65 P62 P64 P63
P312 P321 P3112 P3121 P3212 P3221
P3 P31 P32
P2 P21 C2 C222 C2221
P1

## Slide 55: Pitfalls: alternate indexing
Dangerous ones:
P6x
P4x I4x
P3x R3x P3xXX
http://www.ccp4.ac.uk/html/reindexing.html

## Slide 56: Trick Question: What is the space group?
a = 63 b = 63 c = 63
α = 90 β = 90 γ = 90

## Slide 57: What you know when:
Autoindexing: Lattice (14)
Scaling: Point Group (43)
Refinement: Space Group (84)

## Slide 58: Asymmetric Unit (ASU)
Smallest part of the crystal
that you can use to build up the rest of the crystal
with symmetry operations
Unit Cell
Smallest part of the crystal
that you can use to build up the rest of the crystal
with translation symmetry only
“NCS ASU”
Builds ASU with Non-crystallographic symmetry operations

## Slide 59: Frequency of Space Groups in PDB
13007 | P212121 | 566 | R32 | 191 | P6322 | 74 | P4322 | 36 | P3212
9629 | P21 | 491 | P6522 | 187 | P213 | 71 | P4122 | 30 | P622
5300 | C2 | 474 | P61 | 161 | P6 | 70 | P64 | 24 | F4132
3021 | P21212 | 421 | P65 | 144 | P4212 | 70 | P6222 | 22 | P4332
2543 | C2221 | 353 | P41 | 142 | I23 | 67 | P6422 | 22 | P422
2109 | P1 | 351 | P63 | 132 | F432 | 66 | F222 | 22 | P23
2030 | P43212 | 286 | P31 | 124 | P321 | 63 | P62 | 19 | P3112
1565 | P3221 | 257 | I422 | 115 | I41 | 59 | P4132 | 18 | P4222
1359 | P41212 | 253 | P42212 | 103 | P3 | 46 | P2221 | 18 | I4132
1198 | P3121 | 249 | I4 | 99 | I213 | 43 | P4 | 16 | P432
1147 | I222 | 246 | P43 | 94 | C222 | 43 | I432 | 8 | P4232
825 | R3 | 239 | I4122 | 93 | P2 | 40 | P42 | 3 | P222
620 | P6122 | 193 | P32 | 82 | I212121 | 37 | F23 | 2 | P312

## Slide 60: Twinning?!?
Evil
and pseudo symmetry

## Slide 61: Definitions:
Twinning:
  Two (or more) crystals of the same species joined together with different orientations
Twin law:
  Symmetry operator that rotates one crystal lattice onto the other (common: k,h,-l)
Twin fraction ( α ):
  Mixing ratio: Iobshkl = α Ihkl + (1-α) Ikh-l
Thanks to: Andrea Thorn

## Slide 62: Types of twinning
Thanks to: Andrea Thorn
Merohedral
  Twin law is symmetry operator for lattice,
  but not the true point group
Pseudo-merohedral
  Twin law not symmetry operator for lattice
Non-merohedral
  Lattices don’t perfectly overlap
4. Epitaxial
  Crystals randomly stuck together

## Slide 65: Can you tell by looking?
Macroscopic twin
Disecting apart might give a single crystal!
Microscopic twin
Crystal looks fine, but is twinned.
Images property of Andrea Thorn
and Claudia Egerer-Sieber

## Slide 66: Twinning: how can you tell?

## Slide 67: Make a histogram of your data
Spot intensity
Counts/bin

## Slide 68: Make a histogram of your data
Spot intensity
Counts/bin

## Slide 69: Twinning: how can you tell?
Intensity distribution is abnormal
  H test, L test
Rmerge for higher symmetry
  < 50% → might be twin
  < 10% → could be 50:50 twin
one of the “usual suspects”
  P622, P6, P321, P312, P422, P43
  http://www.ccp4.ac.uk/html/twinning.html
4. can’t solve it

## Slide 70: Find the twin law?
refine in REFMAC
  Automatically checks all possible twin laws!
copy twin law into other programs:
phenix.refine, etc.
Pick Rfree flags in highest symmetry
i.e. P622 if true SG is P3
Do not “twin refine” if not twinned
control: swap non-twin operator

## Slide 71: Twinning: what do I do?
Integrate with low-symmetry SG
  Yes, all possible ones
try to solve it
  Yes, in all possible SGs
  MR: good chance if copies = 1
  MAD: maybe
  S-SAD: no way
  MIR: if you’re lucky
Thanks to: Andrea Thorn

## Slide 72
sample
detector
x-ray beam
scattering

## Slide 73
sample
detector
x-ray beam
scattering

## Slide 74
sample
detector
x-ray beam
scattering

## Slide 75
sample
detector
x-ray beam
scattering

## Slide 76
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 77
to source
to detector
d
d∙sin(θ)
θ
atom #1
atom #2
Bragg’s Law
nλ = 2d sin(θ)

## Slide 78
sample
x-ray beam
anomalous scattering
detector

## Slide 79
sample
detector
x-ray beam
anomalous scattering

## Slide 80
sample
x-ray beam
anomalous scattering
detector

## Slide 81
sample
detector
x-ray beam
anomalous scattering

## Slide 82
sample
detector
x-ray beam
anomalous scattering

## Slide 83
detector
sample
detector
x-ray beam
scattering

## Slide 86
scattering from a structure
sample
detector
beam center
+

## Slide 87
forward Fourier Transform
inverse Fourier Transform
no phase
+

## Slide 88
scattering from a structure
colored by phase
sample
detector
inverse Fourier Transform
+

## Slide 89
scattering from a lattice
colored by phase
sample
detector
beam center
+

## Slide 90
scattering from a lattice
colored by phase
sample
detector
beam center
+

## Slide 91
scattering from a lattice
colored by phase
sample
detector
beam center
+

## Slide 92
scattering from a crystal structure
colored by phase
sample
detector
beam center
+

## Slide 93: lysozyme: real and reciprocal
+
+

## Slide 94: Diffraction from a 3D lattice
real space
reciprocal space
+

## Slide 95: Diffraction from a 3D lattice
real space
reciprocal space
+

## Slide 96: Ewald Sphere
Ewald sphere
(h,k,l)

## Slide 97: Ewald Sphere
Ewald sphere
(h,k,l)
d*

## Slide 98: Ewald Sphere
Ewald sphere
spindle axis
(h,k,l)
d*

## Slide 99: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
(h,k,l)

## Slide 100: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
(h,k,l)

## Slide 101: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)

## Slide 102: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*

## Slide 103: Ewald Sphere
Ewald sphere
spindle axis
Φ circle
diffracted ray
(h,k,l)
d*
λ*
λ*
θ
λ = 2 d sin(θ)